kbg00 | ACSJCA | JCA11.2.5208/W Library-x64 | manuscript.3f (R5.2.i3:5013 | 2.1) 2022/08/03 13:05:00 | PROD-WS-121 | rq_629302 |   7/27/2023 16:24:08 | 20 | JCA-DEFAULT

pubs.acs.org/EF

Review

1  Advances in Catalytic Hydroconversion of Typical Heavy    Carbon

2  Resources under Mild Conditions

3 Xian-Yong Wei,* Xiang Bai, Feng-Yun Ma, Zhi-Min Zong, Wei Zhao, Zhong-Hai Ni, Xing Fan,

4 Lin-Bing Sun, Jing-Pei Cao, Yun-Peng Zhao, Shi-Chao Qi, Jing Liang, Xiao-Ming Yue, Fang-Jing Liu,

5 Wen-Long Mo, Jing-Mei Liu, Yu-Hong Kang, Guang-Hui Liu, Zhong-Qiu Liu, and Li  Li

Cite This: https://doi.org/10.1021/acs.energyfuels.3c01713

Read Online

ACCESS	Metrics & More	Article Recommendations	*sı     Supporting Information

6 ABSTRACT: Low-rank coals, biomass, and heavy petroleum are typical heavy carbon resources, which are currently not efficiently

7 used, and many processes for the current use of the heavy carbon resources cause severe environmental pollution with very limited

8  economic benefits even with a great deficit. Efficiently using the heavy carbon resources can greatly improve the environment and

9  create huge economic benefits. The main difficulty in efficiently using the heavy carbon resources is the high content of  aromatic

10 rings (ARs) and heteroatoms in addition to the insoluble and complex macromolecular structures of the heavy carbon resources.

11 Catalytic hydroconversion (CHC) includes catalytic hydrocracking and subsequent catalytic hydrofining. Many low-rank coals

12 consist of macromolecular species, which are rich in bridged linkages connecting structural units, especially ARs, on which side

13 chains are usually contained. Many ARs, bridged linkages, and side chains contain heteroatoms. Over a proper active catalyst, many

14  bridged linkages and even some side chains can be cleaved, and many heteroatoms outside the ARs can be removed by the   CHC

15  under mild conditions to get soluble portions with relatively simple composition, facilitating subsequent separation to obtain  pure

16  chemicals, especially value-added products, such as condensed aromatics. The remaining economically inseparable species can   be

17 converted to liquid chemicals, especially nonsubstituted and alkyl-substituted cyclanes, by subsequent catalytic hydrofining. Catalysts

18 and catalytically formed active hydrogen play crucial roles in the processes. Mainly based on our investigations, the related advances

19  are reviewed in this work.

# INTRODUCTION

20 Low-rank coals, biomass, and heavy petroleum are typical heavy

21 carbon resources.1−4 Such heavy carbon resources are currently

22  not efficiently  used,  and many  processes,  including catalytic

23  hydroconversion (CHC) at high temperatures, pyrolysis,   and

24 gasification, for the current use of heavy carbon resources cause

25 environmental pollution, e.g., inevitable exhaust gas, wastewater,

26  and  waste  residue,  to  different  extents,  with  very   limited

27 economic benefits even with a great deficit.

28	Efficiently using heavy carbon resources can greatly improve

29  the environment and create huge economic benefits. Most  of

30  heavy carbon resources have high contents of aromatic   rings

31  (ARs), especially condensed ARs, and heteroatoms in addition

32  to  the  insoluble  and  complex  macromolecular   structures,

Received:    May 17, 2023

Revised:	July 14, 2023

causing huge difficulty in their efficient use. When using heavy 33 carbon resources as precursors for producing clean fuels, both 34 ARs and heteroatoms should be removed, but as chemicals, 35 many aromatics, especially condensed and heteroatom-contain- 36 ing aromatics in heavy carbon resources and the soluble portion 37 from converting the heavy carbon resources, are valuable, and in 38 general, the aromatics with more ARs and more heteroatoms are 39

© XXXX American Chemical  Society

A

https://doi.org/10.1021/acs.energyfuels.3c01713

Energy Fuels XXXX, XXX, XXX−XXX

40  more expensive.5  For example, the price of triphenylene  with

41  condensed  4  ARs  is  962  times  that  of  naphthalene   with

42 condensed 2 ARs, and with condensed 3 ARs, the price of

43  acridine is 7.25 times that of anthracene.4

44	CHC   includes   catalytic   hydrocracking   and subsequent

45  catalytic  hydrofining.  Both  low-rank  coals  and   biomass,

46  especially their  insoluble  portions, mainly  consist  of macro-

47 molecular species, which are rich in bridged linkages connecting

48 structural units, especially ARs, on which side chains are usually

49  contained. Since soluble portions in heavy carbon    resources

50 usually consist of numerous organic species, using an insoluble

51  portion as  the reactant  can prevent  the disturbance of     the

52  inherently existing organic species in the soluble portions.6−9

53	Thermal conversions at high temperatures are still the main

54  technologies and the main investigations for utilizing     heavy

55  carbon  resources.  As  mentioned  above,  such   conversions

56 consume large amount of heavy carbon resources with the

57 huge emission of exhaust gas (especially CO2), wastewater, and

58  waste  residue  to  produce  low-value  products.  Developing

59  directional  conversion  technologies,  especially  CHC  under

60  mild conditions, is crucial for smartly converting heavy carbon

61  resources  to  value-added  products,  especially   condensed

62  aromatics, with near-zero emission of exhaust gas, wastewater,

63 and waste residue. Unfortunately, such important investigations

64 were paid less attention compared to thermal conversions. The

65 key scientific issues to be resolved for directional CHC of heavy

66  carbon resources are as follows: (1) How does one    precisely

67 tailor the macromolecular species in the heavy carbon resources

68  to obtain value-added products? (2) What are active hydrogen

The first reason is that macromolecular species in some heavy 101 carbon resources contain weak bridged linkages and bond 102 scissions during the NCHC, e.g., coal pyrolysis, result solely 103 from the thermolysis of weak bridged linkages, so the hydrogen- 104 donating compounds donate their benzylic hydrogen to stabilize 105 radical fragments from the thermolysis of weak bridged 106 linkages,19   as illustrated  in  Scheme  1.  However,  the results 107  s1

Scheme 1. Conventional Consideration on the Role of Hydrogen-Donating Compounds in Promoting the Degradation of Heavy Carbon Resources by Stabilizing the Thermally Produced Radical  Fragments19

from the thermolysis of either 1,2-di(1-naphthyl) ethane or 1,3- 108 diphenylpropane indicate that adding a hydrogen-donating 109 compound inhibit each thermolysis and adding a hydrogen- 110 donating compound with a stronger hydrogen-donating ability 111

20,21

69  species for precisely tailoring the macromolecular species  and

inhibits the thermolysis more  severely.

For example, 1,3- 112

70 how does one effectively produce the active hydrogen species?

71  (3)   Where   are   the  key  positions   to  be   tailored  in   the

72 macromolecular species and what roles do the active hydrogen

73 species play in tailoring the positions? Mainly based on our

74 investigations, the related advances are reviewed in this paper in

75  comparison  with  noncatalytic  hydroconversion  (NCHC) of

76  heavy carbon resources.

diphenylpropane thermolysis is a typical chain reaction and 113

thermally the produced radical fragments, such as benzyl, 114 phenylethyl, and 1,3-diphenylprop-1-yl radicals, play crucial 115 roles in the chain reaction. Benzylic hydrogen provided by a 116 hydrogen-donating compound scavenges the radical fragments 117 and thereby inhibits 1,3-diphenylpropane thermolysis. These 118 facts suggest that scavenging radical fragments by a hydrogen- 119 donating compound could inhibit the NCHC of heavy carbon 120

# THE ROLES OF BENZYLIC HYDROGEN IN THE NCHC

resources.

121

# 77	OF HEAVY CARBON RESOURCES

78  Benzylic hydrogen exists in both heavy carbon resources  and

79  hydrogen-donating compounds used as solvents.   Hydrogen-

80  donating compounds are generally considered to promote the

81  conversion  of  heavy  carbon  resources,  especially   coal

82 liquefaction.10−15  Sheng  et  al.16  investigated  NCHC  of an

83  asphaltene  using tetralin as  a hydrogen-donating compound.

84 Their results showed that the total yield of soluble portion from

85  asphaltene  conversion  reached  70.34%  by  controlling  the

86  reaction conditions. Unfortunately, they did not provide    the

87  detailed analyses, especially detailed molecular composition, of

88 asphaltene and the liquid. In fact, since both asphaltene and the

89 liquid consist of complex organic species, and since tetralin and

90  its  derivates17   could  be  included  in  the  liquid,  getting  the

Another reason is that benzylic hydrogen leaving from a 122

hydrogen-donating compound can attack an ipso-position 123 connecting a arylmethyl group and subsequently cleave the 124 strong >Car−CH2− bond. Such a pathway was first proposed by 125 McMillen et al.22 according to their investigation on the kinetics 126 of diphenylmethane decomposition in tetralin. However, 127 diphenylmethane conversion is less than 0.1% even in 20 h 128 reaction at 400 °C and still negligible even in a stronger 129 hydrogen-donating compound according to their kinetic 130 investigation.  In  fact,  NCHC  of  diphenylmethane  is  very  131

difficult in tetralin even at 430 °C under pressurized H2.23  132

Taking 9,10-dihydroanthracene as an example, as depicted in 133 Scheme 2, thermally cleaving the >Cα-H bond in 9,10- 134 s2 dihydroanthracene  to  produce  H•   and  9-hydroanthr-10-yl   135

radical  is  relatively  easy  because  of  the  relatively  stable  9- 136

91 objective asphaltene conversion and total liquid yield is difficult.

92	Apparently, the hydrogen-donating ability of the hydrogen-

93  donating compounds increases in the order of tetralin  <9,10-

94  dihydrophenanthrene  <9,10-dihydroanthracene,  since  the

95  stability  of  the  resulting  radical  fragments  increases  in the

96  same order, i.e., tetral-1-yl radical <    9-hydrophenanthr-10-yl

97 radical < 9-hydroanthr-10-yl radical.18 The promotional roles of

98 the hydrogen-donating compounds in the NCHC of heavy

99  carbon resources are related to two reasons rather than to any

100 hydrogen-donating compound.

Scheme 2. “Hydrogen Donation” from 9,10- Dihydroanthracene Leading to the Formation of Anthracene24

B	https://doi.org/10.1021/acs.energyfuels.3c01713

Scheme 3. An Example for Cleaving Bridged Linkages by Intramolecular Benzylic Hydrogen Transfer3

Scheme 4. Possible Pathway for the Selective Deoxygenation of Vanillin to 4-Methylguaiacol

Scheme 5. A Chain Reaction from FeS2 Thermolysis to FeS2 Regeneration with H2 to Release H•

137 hydroanthr-10-yl radical, but the resulting H• prefers to abstract

138  benzylic hydrogen in 10-position of 9-hydroanthr-10-yl radical

139  due to the formation of much more stable anthracene   rather

140  than being donated to an ipso-position in a diarylmethane.  In

141  addition, such an intramolecular benzylic hydrogen transfer is

142 more favorable.

143	In some cases, intramolecular benzylic hydrogen     transfer

144  could  result in cleaving  a macromolecular component to     a

s3	145  smaller  compound,  as  Scheme  3  illustrates.  Such  an intra-

146 molecular benzylic hydrogen transfer could proceed at relatively

147  low  temperatures  and  is  desirable  for  producing   valuable

148 condensed arenes, but at temperatures higher than 480 °C,

149  the dehydrogenation from condensed arenes and  subsequent

150  condensation  among  the  condensed  aromatic  radicals    to

151  produce chars are inevitable.

152	Alkanols, such as methanol, ethanol, propan-1-ol, and 2-

153  propanol,  are  also  considered  to  be   hydrogen-donating

154  compounds.25−31  However, since the dissociation energies   of

was completely converted to ethanol-soluble portion and the 168 total yield of aromatics reached 25.5%. Over an acidic catalyst, 169 H+ transfer from 2-propanol to vanillin for selective deoxyge- 170 nation was reported to proceed under mild conditions without 171 H2.42 In this case, H+ could result from the adsorption of oxygen 172 atom in 2-propanol, which is an excellent nucleophilic 173 compound, and subsequent heterolytic cleavage of the −O−H 174 bond. The resulting (CH3)2CHO− adsorbed on the catalyst 175 tends to be converted to acetone by releasing H− from the 176 tertiary carbon. H+ transfer to the oxygen atom in the formyl 177 group of vanillin and subsequent H− abstraction by the benzylic 178

carbon lead to the formation of 4-hydroxymethylguaiacol 179 followed by H+ transfer to the oxygen atom in the −CH2OH 180 group of 4-hydroxymethylguaiacol, dehydration from the 181 protonated −CH2OH group, and H− abstraction by the 182 resulting guaiacylmethylium to produce 4-methylguaiacol 183 (Scheme 4). Noteworthily, transferring H+ to the oxygen atom 184 s4

155 − O−H bonds are much higher than those of ARCH2−H bonds,

156 directly donating H• by cleaving − O−H bonds is difficult. In

157 fact, the alkoxy group in an alkanol is a nucleophilic group, which

158  can attack a carbon atom connected with an oxygen atom and

159  subsequently   cleave   the   >CH2−O−   or   >Car−O− bonds

in both 2-propanol and acetone also consumes H+.

# THE ROLES OF BENZYLIC HYDROGEN, H•, AND BIATOMIC ACTIVE HYDROGEN (H···H) IN THE CHC OF HEAVY CARBON RESOURCES

185

186

187

160 followed by hydrogen transfer from the −OH group in the

161 alkanol to the oxygen atom; i.e., the hydrogen donation of

162  alkanols is induced by alkanolyses.32−40

163	Alkanols are usually used as solvents for the hydroconversion

164 of lignin and its derived monomers. Bai et al.41 examined NiMo/

165  Al-catalyzed hydroconversion of a corncob-derived residue in

166  ethanol under 2.76 MPa of initial hydrogen pressure (IHP)  at

The roles of benzylic hydrogen in the CHC of heavy carbon    188

resources were intensively investigated. According to conven- 189 tional viewpoints,43−49 catalysts promote hydrogen transfer 190 from the hydrogen-donating compound, e.g., tetralin, to the 191 heavy carbon resource and from H2 to the dehydrogenated 192 hydrogen-donating compound, e.g., naphthalene, in addition to 193 the role of the hydrogen-donating compound in scavenging 194

167  320 °C for 7.5 h. Under such reaction conditions, the  residue

radical fragments mentioned above.

195

  - https://doi.org/10.1021/acs.energyfuels.3c01713

196	Indeed, many hydrogen-donating compounds play  positive

197 roles in swelling and dissolving organic matter in heavy carbon

198 resources, but their negative roles in the CHC of heavy carbon

with either a stronger hydrogen-donating ability or a more 236 condensed AR more severely scavenges H•. As a commonly used 237 hydrogen-donating compound, tetralin proved to apparently    238

54

199  resources cannot be ignored. Ouchi and Makabe50  first found

200 the inhibiting effect of tetralin in comparison with decalin, a non-

inhibit both di(1-naphthyl) methane hydrocracking over FeS2 and the reaction of coal macromolecule to oil.51

239

240

201  hydrogen-donating compound, on the CHC of bibenzyl   and

202 benzyloxybenzene at 250 and 400 °C over stabilized nickel.

203  They considered that the inhibiting effect resulted from     the

204 stronger adsorption of tetralin than that of decalin on the surface

205  of stabilized nickel and the main reaction proceeded by direct

206 hydrogen transfer from H2 over the surface of stabilized nickel.

207  Similar suggestion on the main reaction was also proposed by

208  Niu et al.51

In addition to the above defects, both hydroarenes used as   241

hydrogen-donating compounds and their resulting condensed 242 arenes are usually expensive and less volatile, suggesting that 243 they should be recovered as completely as possible after use, but 244 recovering them from a reaction mixture is very energy- and 245 time-consuming. Another problem is that since both hydro- 246 arenes used as hydrogen-donating compounds and their 247 resulting condensed arenes exist in organic matter in heavy 248

55−60

209	FeS2 proved to be active for producing H• by a chain reaction

carbon resources and their soluble products,

distinguishing 249

s5	210  shown  in  Scheme  5  without  any  hydrogen-donating  com-

211 pound52 and H• plays a crucial role in cleaving the >Car−CH2−

their  sources,  i.e.,  whether  they  result  from  the  hydrogen- 250

donating compounds or the heavy carbon resources, is difficult. 251

61−64

212  bridged linkages in diarylmethanes.53  However, FeS2-catalyzed

Some carbon materials, such as activated   carbon

65−67

and 252

•

213  hydrocracking  of  diphenylmethane  in  decalin  at  400     °C

carbon black,

also catalyze the formation and transfer of H

253

214  indicated that adding a hydrogen-donating compound, such as

215  tetralin,  9,10-dihydrophenanthrene,  and 9,10-dihydroanthra-

216  cene, inhibited diphenylmethane hydrocracking and adding   a

217  stronger  hydrogen-donating  compound  inhibited  diphenyl-

218  methane  hydrocracking  severer.24   Diphenylmethane  hydro-

219  cracking was more inhibited by adding the hydrogen-donating

by homogeneously splitting H−H bond in H2. Adding sulfur   254

promotes di(1-naphthyl) methane hydrocracking over an 255 activated carbon due to the formation of H2S by the reaction 256 of H2 with the added sulfur over the activated carbon and the 257 much weaker H−S−H bond than H−H bond, and the 258 synergistically  increased  di(1-naphthyl)  methane  conversion 259

61

220  compound-derived condensed arenes, i.e., naphthalene,   phe-

increases with raising the reaction temperature up to 350 °C.

260

221 nanthrene, and anthracene, and diphenylmethane conversion in

Previous  investigation  on  the  CHC  of  α,ω-diarylal-   261

222  the  condensed  arenes  added  decreased  in  the  order      of

kanes

53,63,66,68

indicated that the effectiveness of   H•

transfer 262

223  naphthalene > phenanthrene > anthracene, being the same as

224  the order of the resulting hydrogen-donating compounds, i.e.,

for cleaving bridged linkages connecting ARs over FeS2  under 263

mild conditions not only depended on the H•-accepting ability, 264

21,69

225 tetralin >9,10-dihydrophenanthrene >9,10-dihydroanthracene,

in terms of superdelocalizability (Figure  1),

of an AR, but 265 f1

226  since the more condensed arenes more strongly adsorb on the

was also related to the stability, in terms of resonance energy   266

70

227  catalyst  surface,  and  there  are  equilibriums  between     the

(Figure 2),

of the leaving arylalkyl or diarylalkyl radical.

267 f2

228  hydrogenation of condensed arene to its resulting   hydrogen-

According to the CHC of α,ω-diarylalkanes at 300 °C over   268

68

FeS2,

only very small amount of biphenyl was converted to   269

229  donating compound, e.g., anthracene to   9,10-dihydroanthra-

230  cene,  and  the  dehydrogenation  of  a    hydrogen-donating

231  compound to its corresponding condensed arene, e.g.,    9,10-

232  dihydroanthracene to anthracene, under pressurized H2     over

233  FeS2. Such an intramolecular hydrogenation and dehydrogen-

234 ation mainly consumes H• rather than donates H• to another

s6	235  molecule (Scheme 6). These results indicate that  an   additive

Scheme 6. Intramolecular H• Transfer between 9,10- Dihydroanthracene and Its Dehydrogenated  Products4

cyclohexylbenzene, while both bibenzyl and 1,3-diphenylpro- 270 pane were not converted due to the weak H•-accepting ability of 271 benzene ring (BR) and the resulting labile phenylethyl and 272 phenylpropyl radicals. Under the same conditions, 1,2-di(1- 273 naphthyl) ethane hydrocracking is not significant and the main 274 products are partially hydrogenated derivates due to the much 275 stronger H•-accepting ability of naphthalene ring (NR) than 276 that of BR but the still labile naphthylethyl radical. Bi(1- 277 naphthyl) cannot be directly hydrocracked under the same 278 conditions because of the resulting extremely labile phenyl 279 radical, but both naphthalene and tetralin were detected from 280 the CHC of bi(1-naphthyl) since H• transfer to the ipso-position 281 of a NR in bi(1-naphthyl) and subsequent H• transfer to the 282 same NR produced 1-(tetralyl) naphthalene, and subsequent H• 283 transfer to the ipso-position of NR in 1-(tetralyl) naphthalene  284

produced naphthalene and tetralin.

285

Either iron sulfide- or nickel sulfide-catalyzed reaction of 9,10- 286 diphenylanthracene primarily proceeds by H• transfer to the 9- 287 and 10-positions of 9,10-diphenylanthracene, producing 288 (9R,10R)-9,10-diphenyl-9,10-dihydroanthracene as the main 289 product and (9R,10S)-9,10-diphenyl- 9,10-dihydroanthracene   290 as the byproduct71,72 because of the much larger super- 291 delocalizability of 9- and 10-positions than other positions 292 (Figure 1 and Scheme 7). H• can attack the 10-position of the 293 s7 intermediate 9,10-diphenyl-9-hydroanthryl radical via either the 294 same direction as the H• transfer to 9-position of 9,10- 295 diphenylanthracene or the  opposite direction. In the  case of  296 the H• transfer via the same direction, the added H• in the 9- 297 position tends to be abstracted by the adding H•, while in 298

  - https://doi.org/10.1021/acs.energyfuels.3c01713

Figure 1. Superdelocalizabilities of carbon atoms in different positions of the typical arenes.21,69

Figure 2. Resonance energies (kJ mol−1) of some benzylic radicals.70

Scheme 7. Reaction Pathway for H• Transfer to 9,10-

and  (9R,10S)-9,10-diphenyl-9,10-dihydroanthracene  (Scheme 312

Diphenylanthracene71,72

7).

313

The CHC of 1-benzylnaphthalene at 300 °C over FeS2 314 predominantly proceeds via H• transfer to the ipso-position of 315 NR in 1-benzylnaphthalene also due to the much stronger H•- 316 accepting ability of NR than BR.53  However, 2-benzylnaph- 317

thalene and two 2-benzyltetralins were unexpectedly detected. 318 Their formation should be ascribed to the addition of the 319 relatively reactive benzyl radical, the leaving radical from the NR 320 via NR-CH2BR bond cleavage, to the 2-position of the NR. 321 Similar to FeS2, activated carbon predominantly catalyzes the 322 partial hydrogenation of condensed arenes. The reactivities of 323 condensed arenes toward the partial hydrogenation were found 324 to  be  closely  related  to  the  H•-accepting  abilities  of  the    325

condensed arenes.63

326

299 another case the adding H• cannot abstract the added H• so that

300 the transhydrogenation to 9,10-diphenylanthracene is predom-

The above results suggest that cleaving bridged linkages in 327 heavy carbon resources by H• transfer under mild conditions 328 over both metal sulfides and carbon materials is selective to 329 some extent. Using a tetrahydrofuran/methanol mixture− 330 insoluble portion of Pingshuo bituminous coal as an example, 331 its CHC over an iron−sulfur system and NCHC at 300 °C in   332

73

301  inant.   H•    transfer   to   either  (9R,10R)-9,10-diphenyl-9,10-

cyclohexane were investigated.

As a result, the CHC produced 333

302  dihydroanthracene or (9R,10S)-9,10-diphenyl-9,10-dihydroan-

303 thracene is difficult due to the small superdelocalizability of the

304  BRs  in  (9R,10R)-9,10-diphenyl-9,10-dihydroanthracene  and

305  (9R,10S)- 9,10-diphenyl-9,10-dihydroanthracene. In particular,

306  H•   transfer  to  the  *C  in  (9R,10R)-9,10-diphenyl-  9,10-

307  dihydroanthracene   and  (9R,10S)-9,10-diphenyl-9,10-dihy-

308  droanthracene is the most difficult, since the   superdelocaliz-

309 ability of *C is smallest and the transferring H• can be easily

310  abstracted by the  benzylic hydrogen, which is also a    tertiary

311  hydrogen, in (9R,10R)-9,10-diphenyl-9,10- dihydroanthracene

much more anthracene and 9,10-dihydroanthracene than the   334

NCHC. In addition, the yield of 9,10-dihydroanthracene is 335 much lower than that of anthracene from the NCHC, while the 336 yield of 9,10-dihydroanthracene is appreciably higher than that 337 of anthracene from the CHC. The insoluble portion should 338 contain or even rich in anthracene ring, and some ARs could be 339 connected with a macromolecular group (MMG)-substituted   340

BRCH2-, BRO-, BRS-, and/or BRNH- group. H• transfer to the 341

ipso-position in the anthracene ring induced the cleavage of the 342

MMG-substituted  BRCH2-anthracene  ring,  BRO-anthracene 343

  - https://doi.org/10.1021/acs.energyfuels.3c01713

344 ring, BRS-anthracene ring, and/or BRNH-anthracene ring, and

345  thereby released anthracene, which can be easily converted  to

s8	346  9,10-dihydroanthracene by subsequent H• transfer (Scheme 8).

Scheme 8. Possible Pathway for the Release of Anthracene and 9,10-Dihydroanthracene from the CHC of a

1,2,3,4,5,6,7,8-octahydroanthracene as the byproducts under 5 371 MPa of IHP at 150 °C over Ni/ZSM-5 for 5 h.77 Interestingly, all 372 the products kept the central BR unhydrogenated, indicating 373 Ni/ZSM-5 specifically catalyzed H···H transfer to 9,10- 374 diphenylanthracene. In other words, 9,10-diphenylanthracene 375 hydrogenation can be used to justify the type of hydrogen 376

Tetrahydrofuran/Methanol  Mixture−Insoluble  Portion of

transfer, i.e., H• or H···H transfer.

377

Pingshuo Bituminous Coal over an Iron−Sulfur System

Ni/attapulgite powder is also active for arene hydrogenation 378

under mild conditions.78 Under 4 MPa of IHP for 4 h, 379 anthracene was completely converted to perhydroanthracenes at 380 175 °C, but anthracene conversion dropped to <75% with 9,10- 381 dihydroanthracene as the main product at 300 °C, clearly 382 indicating that saturated hydrogenation should not proceed at 383 high temperatures. Similar to other ultrafine metals, Ni/ 384 attapulgite powder also activates H2 to H···H to effectively 385 hydrogenate anthracene to perhydroanthracenes at low temper- 386 atures, but at high temperatures H···H bond tends to be 387 thermally cleaved to produce H•, which transfer to anthracene 388 predominantly yields 9,10-dihydroanthracene, and there is an 389 equilibrium between anthracene hydrogenation and 9,10- 390 dihydroanthracene  dehydrogenation  by  the  H•   transfer,  as  391

347	Different from metal sulfides, ultrafine metals mainly activates

depicted in Scheme 9.78

# THE ROLES OF H+ AND H···H IN THE CHC OF HEAVY CARBON RESOURCES

•

392 s9

393

348  H2    to   H···H   under   mild   conditions.74,75   Di(1-naphthyl)

There are three problems for H

transfer to specifically cleave 394

349  methane  was  completely  converted  to  its    hydrogenated

350  products, which mainly consist of naphthylmethyltetralins and

351  ditetralylmethanes,  under  10  MPa  of  IHP  at  300  °C over

352  ultrafine  iron,  while  adding  sulfur  inhibited  di(1-naphthyl)

353  methane hydrogenation but promoted di(1-naphthyl) methane

354  hydrocracking.74   The  main  products  from 9,10-diphenylan-

355 thracene hydrogenation are 9,10-diphenyl-1,2,3,4-tetrahydroan-

356  thracene  and  9,10-diphenyl-1,2,3,4,5,6,7,8-octahydroanthra-

357  cene  over ultrafine  metals  under mild  conditions,  since the

358 main active hydrogen is H···H and its transfer to 9- and 10-

359 positions is very difficult due to the much smaller distance

360 between the two hydrogen atoms in H···H than that between the

361  two carbon atoms in 9- and 10-positions of  9,10-diphenylan-

362  thracene.71,72 Ni/ZSM-5 prepared using nickel tetracarbonyl as

363  the  precursor  for  nickel  is  highly  active  for  completely 364 hydrogenating polymethylbenzenes,76 naphthalene,  phenan- 365 threne, and anthracene under 6 MPa of IHP at 160−220 °C

366  and also effective for catalyzing coal tar hydrogenation.77 9,10-

367  Diphenylanthracene  was  hydrogenated  to   9,10-diphenyl-

368  1,2,3,4,5,6,7,8-octahydroanthracene as the main product along

369  with  9,10-dicyclohexylanthracene,  9,10-dicyclohexyl-1,2,3,4-

370  tetrahydroanthracene,  and  9-cyclohex-  cyl-10-phenyl-

bridged linkages. The first one is the difficulty in significantly 395 increasing the H• concentration, because such an increase 396 enhances the possibility for scavenging the H•  species by their 397

collision to produce H2. The second one results from the partial 398

hydrogenation by H• transfer, e.g., the CHC of di(1-naphthyl) 399

methane to naphthylmethyltetralins and bi(tetralyl) meth- 400 anes,54,74 1-benzylnaphthalene to benzyltetralins,53 and 1,2- 401 di(1-naphthyl) ethane to naphthylethyltetralins and 1,2- 402 (ditetralyl) ethanes.68 In particular, H• transfer to condensed 403 arenes usually produces multiple partially hydrogenated 404 products; e.g., H• transfer to 2,3-naphthacene over an activated 405 carbon produced seven partially hydrogenated products.62 406 Apparently, separating any  partially  hydrogenated  product  407 from such a mixture is not easy. The last one is caused by the 408 scavenging effect of benzylic hydrogen on H• transfer, e.g., as 409 mentioned above, H• transfer over either a metal sulfide or an 410 activated carbon to the ipso-position of di(1-naphthyl) methane 411 induces di(1-naphthyl) methane hydrogenation.52−54,74,75 412 However, as Scheme 10 demonstrates,79 the abstraction of 413 s10 benzylic hydrogen from the − CH2− in di(1-naphthyl) methane 414

by H•  and subsequent H•  addition to the resulting −•CH−  415

should also be considered. Such an abstraction and addition 416

Scheme 9. Anthracene Hydrogenation at 175 and 300 °C over Ni/Attapulgite Powder78

F	https://doi.org/10.1021/acs.energyfuels.3c01713

Scheme 10. Possible Mechanism for Scavenging H• by Benzylic  Hydrogen  in Di(1-naphthyl)methane79

genation at 300 °C, suggesting that the new solid acid is active 448 for heterolytically splitting H2 to mobile H+ and immobile H− 449 attached on the surface of the new solid acid and H+ transfer to 450 the ipso-position of di(1-naphthyl) methane induces di(1- 451 naphthyl) methane hydrocracking. Interestingly, the yield of 452 naphthalene is appreciably higher than that of 1-methylnaph- 453 thalene, implying that the demethylation appreciably proceeded 454

over the new solid acid.

455

417 consumed H• without contribution to di(1-naphthyl) methane

418 hydrocracking.

419	Different from H•  transfer, H+  transfer does not    abstract

420  benzylic hydrogen and scavenging H+  does not occur by   the

The CHC of an insoluble portion from Lingwu bituminous 456 coal was also investigated at 300 °C over the new solid acid.8 457 Compared to the NCHC, the CHC of the insoluble portion 458 produced much more arenes and phenols. Noteworthily, ca. 459 66.1% of the arenes is due to diphenylmethane, further 460 suggesting that some arenes can be released in a high yield 461 from the CHC of a heavy carbon resource similar to the CHC of 462

73

421  collision of H+  species to provide a possibility for significantly

the insoluble portion from Pingshuo bituminous coal.

Most of 463

422  increasing the H•  concentration. For example, the acidities  of

423 carborane acids80 and a mixture called magic acid81 consisting of

424  equimolar parts of FSO3H and SbF5 are 1 million and 1 billion

the  resulting  phenols  are  alkyl-substituted  phenols.  In  the 464

insoluble portion from Lingwu bituminous coal, as Scheme 11 465 s11

exhibits, diphenylmethyl group (DPMG) could be connected   466

+

425 times, respectively, stronger than that of concentrated H2SO4. In

with  a  MMG-substituted  anthracene  ring  (MMGSAR). H

467

426 addition, two or more H+ species cannot simultaneously attack

427 the same AR to avoid the AR hydrogenation.

428	Unfortunately, the practical application of both   carborane

429 acids and magic acid in catalyzing the hydroconversion of heavy

430  carbon resources is  difficult due to the extreme difficulty    in

431  synthesizing carborane acids and too severe corrosiveness   of

432 magic acid. Conveniently preparing a less corrosive, recyclable,

433  and  highly  active  catalyst  for  heterolytically  splitting  H2 to

434 effectively release mobile H+ is one of our ultimate targets. We

435  believe that such a  catalyst greatly facilitates the     directional

436 CHC of heavy carbon resources under mild conditions.

437	A new solid acid was prepared by ultrasonically impregnating

438  isometric pentachloroantimony and trimethylsilyl trifluorome-

439  thanesulfonate into an activated carbon.82  Multiple    analyses

440  reveal  the  strong  interactions  among pentachloroantimony,

441  trimethylsilyl   trifluoromethanesulfonate,   and   the activated

442 carbon in the new solid acid and suggest that the new solid

transfer to the ipso-position of the MMGSAR induces the 468

cleavage of the DPMG-MMGSAR bond, releasing diphenylme- 469 thylium followed by the abstraction of H− by diphenylmethy- 470 lium from the surface of H−-attached new solid acid. Similarly, 471 the −CH2−O- bridged linkage connecting an alkyl-substituted 472 BR with a MMGSAR could be cleaved by H+ transfer to the 473 oxygen atom in the bridged linkage to release alkyl-substituted 474 phenols. Significantly higher yields of arenes and arenols were 475 also released from the CHC of insoluble portion obtaining from 476

Piliqing subbituminous coal over a highly active magnetic solid 477 superacid compared to the NCHC at 300 °C.83 More 478 interestingly, significantly high yield of mesitylene, a value- 479 added compound having many important applications, were    480

released from the CHC of insoluble portions obtaining from 481 Piliqing subbituminous coal,82 Hefeng subbituminous coal,84 482 Huozhou lignite, and Shaerhu lignite,85 and all the coal samples 483 were collected from Xinjiang Uyghur Autonomous Region, 484

443  acid  exhibits  an  appreciably  stronger  acidity  than     either

China.

485

444  pentachloroantimony/activated  carbon  or  trimethylsilyl  tri-

445 fluoromethanesulfonate/activated carbon. Over the new solid

446  acid, di(1-naphthyl) methane was specifically hydrocracked  to

447  naphthalene  and  1-methylnaphthalene  without  NR  hydro-

Naomaohu lignite is also a low-rank coal collected from 486 Xinjiang Uyghur Autonomous Region, China. Its CHC was 487 ultrasonically extracted with isometric carbon disulfide/acetone 488 mixed solvent (MS) and the resulting insoluble portion was 489

Scheme 11. Possible Pathways for Releasing Diphenylmethane and Alkyl-Substituted Phenols from the CHC of the Insoluble Portion Obtained from Lingwu Bituminous Coal over the New Solid Acid8

G	https://doi.org/10.1021/acs.energyfuels.3c01713

490  isolated  into  light  and  heavy  insoluble  portions  in carbon

491  tetrachloride.  The  light  insoluble  portion  was  subjected to

492 NCHC and CHC in cyclohexane at 160 °C under 4 MPa of IHP

493  for 12 h. Trifluoromethanesulfonic acid supported on an acid-

494  treated attapulgite was used as the catalyst for the CHC. As  a

495 result, the yield of soluble portion from the CHC is 60.0%, while

496 the yield (1.8%) of soluble portion from the NCHC is negligible.

497 The predominant products from the catalytic hydroconversion

ring. The >CH−OH2+ bond cleavage to produce H2O and 527 perhydroanthr-9-ylium is relatively easy because of the resulting 528 relatively stable perhydroanthr-9-ylium. Then, perhydroanthr-9- 529 ylium can abstract H− from the surface of H−-attached Ni/solid 530 acid to yield perhydroanthracene. By the synergic H+ and H···H 531 transfer, the CHCs of other heavy carbon resources, including 532 extracts from an oil sludge89 and Jinjitan subbituminous coal,91 533 and an organic waste oil91,92 to cyclanes over Ni/solid acids were 534

498  are  oxygen-containing  organic  compounds,  especially   4-

also achieved.

535

499 methylpent-3-en-2-one and 4-hydroxy-4-methyl-pentan-2-one,

500 suggesting that the cleavage of >Cα−Oβ− and >Cβ−Oα− bonds

501 in the light insoluble portion significantly proceeded during the

502  CHC.86    Oxygen-containing  organic  compounds  are   also

503  predominant from the CHC of an alkali lignin over Ni/Hβ.87

504	Nickel supported on solid acids proved to be the bifunctional

505 catalyst for the CHC of heavy carbon resources to cyclanes.88−92

506 Earlier investigation focused on the CHC of the methanol-

507 soluble portion, mainly consisting of    heteroatom-containing

508  organic  compounds  with  small  amounts  of  chain  alkanes,

509 alkenes, and arenes, from Xiaolongtan lignite in cyclohexane at

510  200 °C over Ni/Z5A.88  After the catalytic   hydroconversion,

511  arenes  and  almost  all  the  heteroatom-containing    organic

512  compounds  were  converted  to  chain  alkanes  and cyclanes.

513  Especially,  the  resulting  cyclanes  account  for  70%  of  the

514 products, while ca. 45% of the methanol-soluble portion is

515 arenols, which was completely converted to cyclanes.

Chen et al.93 investigated CHC of butyl levulinate, an 536 important biomass-derived compound, to γ-valerolactone over 537 Cu0.5Ni1Co3B. Their results exhibited that the conversion of 538 butyl levulinate and γ-valerolactone reached up to 99.7% and 539 89.5%, respectively, under 3 MPa of H2 at 200 °C for 3 h, but 540 they did not explain the reaction pathway. As found by Scotti et 541 al.94 that very small particles (less than 5 nm) of metallic Cu 542 could exhibit catalytically relevant Lewis acidity. So, the 543 activation of H2  to H···H and heterolytic cleavage of H···H to 544

relatively  mobile  H+    and  immobile  H−    attached  on  the   545

Cu0.5Ni1Co3B surface could also proceed. There are three 546 oxygen atoms in butyl levulinate and the conversion of butyl 547 levulinate to γ-valerolactone suggests that H+ preferentially 548 attacks the oxygen atom in acetyl group of butyl levulinate 549 followed by abstracting H− from the catalyst surface by the 550 protonated butyl levulinate to produce butyl 4-hydroxypenta-  551

+

s12	516	As illustrated in Scheme 12, Ni/solid acid     simultaneously

noate, H

transfer to the oxygen atom in hydroxy group of butyl 552

517 activates H2 to H···H and splits both H2 and H···H to mobile H+

4-hydroxypentanoate, dehydration from the protonated butyl 4- 553

hydroxypentanoate, and the formation of the >C*H−O− bond 554

(Scheme 14).

555 s14

Scheme 12. Catalysis of a Ni/Solid Acid in Activating H2 to

+

Furfural is another important biomass-derived compound and 556

H···H and Splitting both H2 and H···H to Mobile H

−

and

89

mainly obtained from corncob.95  It can be selectively hydro-    557

Immobile H

Attached on the Surface of Ni/Solid Acid

genated to furan-2-ylmethanol, (tetrahydrofuran-2-yl) meth- 558 anol, 2-methylfuran, and cyclopentanone,96,97 and among them 559 furan-2-ylmethanol has multiple applications in producing 560 resins, biofuels, fuel additives, lysine, vitamin C, levulinic acid, 561 alkyl levulinates, and γ-valerolactone.98−100 Thereby, selective 562 catalytic hydrogenation of furfural to furan-2-ylmethanol 563 received great attention.95−122 In light of practical applications, 564 completely converting furfural to furan-2-ylmethanol is of great 565 importance to avoid the troublesome separation of target 566 product furan-2-ylmethanol from the reaction mixture, includ- 567

518  and immobile H−  attached  on the  surface  of  Ni/solid  acid.

519 Taking anthracen-9-ol as an example, H+ transfer to the oxygen

520  atom  in  anthracen-9-ol  cannot  cleave  the  >Car−OH bond

521  because of the extreme labile leaving group, i.e., anthr-9-ylium

s13	522 (Scheme 13). However, the added H+  on the oxygen atom

523 avoids the Ni/solid acid poisoning by the oxygen atom and

524  ensures the saturated hydrogenation of the anthracene ring  in

525 the protonated anthracen-9-ol to a protonated perhydroan-

526  thracen-9-ol via subsequent H···H transfer to the  anthracene

ing the reactant furfural and its by products. Furfural 568 hydrogenation of furan-2-ylmethanol can significantly proceed 569 at near room temperature over rare earth element- or novel 570 metal-containing catalysts (entries 2, 6, 10, 14, and 17 in Table 571 t1 1), but the complete conversion of furfural to furan-2- 572 t1 ylmethanol was achieved only over Pt(3) Co(3)/C (Entry 6 573 in Table 1) in these cases and the high catalyst cost prevents the 574 catalysts from practical applications. The main solvents used 575 under optimal conditions include alkanols (entries 1, 4, 5, 7−9, 576

Scheme 13. Synergic H+ and H···H Transfer during the CHC of Anthracen-9-ol to Perhydroanthracene over a Ni/Solid Acid89

Scheme 14. Possible Pathway for the CHC of Butyl Levulinate to γ-Valerolactone

Table 1. Comparison of the Catalytic Hydrogenation of Furfural to Furan-2-ylmethanol under Different Conditionsa

optimal condition

entryref

| catalyst solvent IHP (MPa) temperature (°C) time (h) FC (%) FMS (%) AH |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Co/SBA-15 | ethanol | 2 | 150 | 1.5 | 96 | >95 | NC |
| Ru/UiO-66 | water | 0.5 | 20 | 4 | 94.9 | 100 | NC |
| Pd5%-Cu5%/MgO | water | 0.8 | 130 | 0.9 | 100 | 99 | NC |
| γ-Fe2O3@HAP | IP | 0 | 180 | 10 | 96.2 | 91.7 | NC |
| Cu/AC−SO3H | IP | 0.4 | 105 | 2 | >99.9 | >99.9 | H+ |
| Pt(3) Co(3)/C | water | 0.1 | 35 | 10 | 100 | 100 | H+ |
| Cu/MgAlO | ethanol | 4 | 150 | 3 | >99 | >99 | NC |
| Ni/NAC-1−1073 | IP | 4 | 80 | 3 | 100 | ca. 100 NC |  |
| CuCo0.4/C-873 | ethanol | 3 | 140 | 1 | 98.7 | 97.7 NC |  |
| Co/ZrLa0.2Ox | water | 2 | 40 | 10 | 98 | 95 H+ |  |
| Zr(OH)4 | IP | 0 | 170 | 2.5 | 100 | 98.9 H+ |  |
| Ni3Fe1/SiO2 | methanol | 3.4 | 140 | 2 | 100 | 96.5 NC |  |
| Ni@N/C-g-800 | THFAS | 2 | 140 | 6 | 99 | 98 NC |  |
| Ir/H@MoOx-400 | water | 2 | 30 | 6 | >99 | >99 H+ |  |
| Co@CPNs1.5−1.5−4 | IP | 3 | 180 | 2.5 | 99 | 99 NC |  |
| Cu/MgO-Al2O3 | IP | 0 | 210 | 1 | 100 | 89.3 H+ |  |
| Pt(3) Ni(3)/C | water | 2 | 35 | 12 | 99 | 93 NC |  |
| Cu/C | IP | 2 | 175 | 2 | 99.8 | 100 H+ |  |
| HT_MgFe-3 | IP | 0 | 170 | 6 | ca. 97 | ca. 90 H− |  |
| Cu−Co/C | IP | 3 | 200 | 2.5 | 100 | 97.2 H+ |  |
| Co−N−C-700 | FA | 0 | 150 | 6 | 100 | 99.9 H+ |  |
| Ni0.09Zn/NC600 | IP | 2 | 170 | 2 | 99.7 | 100 H+ |  |
| Co17Zn/NC600 | ethanol | 2 | 125 | 2.5 | 100 | 100 H+ |  |

1100

2101

3102

4103

5104

6105

7106

8107

9108

10109

11110

12111

13112

14113

15114

16115

17116

18117

19118

20119

21120

22121

23122

aFC, FMS, AH, NC, IP, THFAS, and FA denote furfural conversion, furan-2-ylmethanol selectivity, active hydrogen, not clarified, 2-propanol, tetrahydrofuran aqueous solution, and formic acid, respectively.

577 11, 12, 15, 16, 18−20, 22, and 23 in Table 1), formic acid (entry

578  21 in Table 1), tetrahydrofuran aqueous solution (entry 13   in

579 Table 1), and water (entries 2, 3, 6, 10, 14, and 17 in Table 1).

# THE ROLES OF H− AND H···H IN THE CHC OF HEAVY CARBON RESOURCES

600

Superbases  were  extensively  used  for  catalyzing  organic   601

580  The heterolytic cleavage of H2 and the transfer of the resulting

581  H+  to the oxygen atom in the −CHO group of furfural   were

synthesis123−126

and CO2 capture,

127,128

but only a few attempts 602

582  clarified to be key steps for furfural hydrogenation to furan-2-

583  ylmethanol (entries 5, 6, 10, 14, and 18−23 in Table 1)   under

584  pressurized H2. Without H2, the transfer of H+  from a solvent

585 also induced furfural hydrogenation to furan-2-ylmethanol over

586  an acidic catalyst (entries 4, 11, 16, 19, and 21 in Table  1).

587	Taking 2-propanol as an example, similar to H+ transfer from

588  2-propanol  to  vanillin  displayed  in  Scheme  5,  the   strong

589 adsorption of the oxygen atom in the hydroxy group of 2-

590  propanol  on  the  surface  of  an  acidic  catalyst  leads  to the

591 heterolytic cleavage of −O−H bond to release H+ and retain the

592  isoproxy anion on the catalyst surface. The H−  transfer to the

have been tried on the application of superbases in the CHC of 603 LRMCs129−134 and heavy carbon resources.130−135 Since the 604 C−O bridged bonds (COBBs), such as ARCH2O−CH2AR, 605 AROCH2AR, and ARO-AR, are the predominant COBBs in   606

lignites,136−138  insight into the catalytic hydroconversions of 607

LRMCs, such as oxybis(methylene) dibenzene, benzyloxyben- 608 zene, and oxidibenzene with COBBs, has become a powerful 609 tool to understand the mechanisms for selectively cleaving 610 COBBs and hydrogenating AR in lignites at molecular level.10,12 611 Among the COBBs, BRO-BR bond (360 kJ mol−1) in 612 oxidibenzene is the strongest,139,140 so the research gaining 613 insight into the cleavage of COBB in oxidibenzene has attracted 614

593  oxygen  atom  in  the  hydroxy  group  of  furfural    produces

extensive attention.

615

594  furyl(hydroxy) methylium, followed by H−  abstraction    from

595 the tertiary carbon in the isoproxy anion by furyl(hydroxy)

596  methylium  to  generate  furan-2-ylmethanol.   Co17Zn/NC600

597  proved to be an effective non-novel catalyst  for    completely

598 hydrogenating furfural to furan-2-ylmethanol (entry 23 in Table

599 1).

Our earlier investigation used oxidibenzene, benzyloxyben- 616 zene, and oxybis(methylene) dibenzene as lignin-related model 617 compounds (LRMCs) and compared the activities and 618 selectivities of Ni/γ-Al2O3, Mg2Si/γ-Al2O3, and Ni−Mg2Si/γ-  619

Al2O3 for the CHC of the LRMCs.129 As a result, Ni−Mg2Si/γ- 620

Al2O3  proved  to  be  the  most  effective  for  converting   621

I	https://doi.org/10.1021/acs.energyfuels.3c01713

622 oxidibenzene to cyclohexane, benzyloxybenzene to cyclohexane 623 and methylcyclohexane, and oxybis(methylene) dibenzene to 624 methylcyclohexane at 240 °C by the synergic transfer of H− and 625 H···H to the LRMCs. The CHC of oxidibenzene over Mg2Si/γ- 626 Al2O3  only  produced  benzene  and  phenol,  and  phenol 627 conversion to benzene also proceeded without H···H trans- 628 fer,129,130  while oxidibenzene was not converted at all over

As the main compounds in the MS-soluble portion (MSSP) 649 from Piliqing subbituminous coal, nonsubstituted arenes were 650 effectively converted to nonsubstituted cyclanes133 and a series 651 of normal alkanes were also released56  during the CHC at 240  652

°C over Ni−Mg2Si/γ-Al2O3, while substituted phenols and 653 benzenediols are the main products from the CHC of 654 Xiaolongtan lignite at 300 °C over Fe O @SiO @mSiO .134  655

3    4	2	2

629  trifluoromethanesulfonic acid/attapulgite powder due to   the

The  much  weaker  alkalinity  of  Fe3O4@SiO2@mSiO2   than 656

630  resulting extremely labile phenylium from H+  transfer to   the

Mg Si/γ-Al O

and the lack of metallic nickel in Fe O @SiO @ 657

2	2    3

3    4	2

s15	631  oxygen atom  in  oxidibenzene  (Scheme  15).130  Although the

mSiO2

lead to the difficulty in deoxygenation and subsequent  658

BR hydrogenation of the resulting substituted phenols and 659

Scheme 15. Difference between H− Transfer and H+ Transfer

benzenediols.

660

in Cleaving the >Car−O− Bond in Oxydibenzene

Wang et al.142 investigated the catalytic hydrogenolysis of a 661 poplar wood sawdust-derived lignin over a NiAl alloy. Their 662 results showed that 18.9% and 55.5% of the lignin were 663 converted to monomers and oligomers, respectively, in 0.2 mol 664 L−1 of NaOH aqueous solution under 2 MPa of IHP at 220 °C 665 for 3 h. They tried to reveal the mechanism for the catalytic 666 hydrogenolysis   by   examining  the   depolymerization   of  2- 667

phenoxy-1-phenylethanol over the NiAl alloy in NaOH aqueous 668 solution under pressurized H2 at 110 °C for 1 h. As a result, 669 phenol and 1-phenylethan-1-ol were detected as the main 670 products. In the reaction systems of both catalytic hydro- 671 genolysis of the lignin and 2-phenoxy-1-phenylethanol depoly- 672 merization, in addition to H···H resulting from H2 activation by 673

the NiAl alloy, the main active hydrogen should be H−  rather  674

than H+, due to the use of NaOH aqueous solution as the 675 solvent. As Scheme 16 illustrates, the reaction of HO− in the 676 s16 NaOH aqueous solution with H···H produces H− and H2O, and 677 the resulting H− tends to attack the *C, which is positively 678 charged, to cleave the *C−O- bond and produce 1-phenylethan- 679

1-ol and phenoxy anion, followed by the reaction of the phenoxy 680

+

632  >Car−O− bond is much stronger than the −CH2−O− bond in

anion  with  Na

to  produce  sodium  phenolate  and  the   681

633 benzyloxybenzene, H− transfer only induces the cleavage  of 634 >Car−O− bond in benzyloxybenzene because the Car in >Car− 635 O− is most positively charged141 and much more tends to be 636  attacked by H−131  under mild conditions.

acidification of sodium phenolate with HCl aqueous solution   682

to produce phenol and NaCl. The main problem of such a 683 process for future practical application is the consumption of 684 NaOH and HCl aqueous solution along with the production of 685

637	The  NCHC  and  CHC  of  MS-insoluble  portion (MSISP)

NaCl-containing wastewater.

686

638 from Naomaohu lignite were compared at 240 °C under 4 MPa 639 of IHP.56 The yield of soluble portion from the CHC over Ni− 640 Mg2Si/γ-Al2O3 is much higher than that from the NCHC and 641 the main products in the soluble portion from the CHC are 642 chain alkanes and cyclanes, while the NCHC mainly produced 643 arenes and oxygen-containing organic compounds. In contrast, 644 the CHC of MSISP from Naomohu lignite mainly produced 645 oxygen-containing organic compounds over a Ni-free magnetic 646 solid superbase,132 further illustrating that the synergic transfer 647 of H− and  H···H  is  crucial  for  deoxygenation  under mild 648 conditions.

Aqueous coprecipitation followed reduction with H2  is an    687

important approach for preparing highly active supported 688 metallic catalysts, in which ultrafine metal particles are highly 689 dispersed onto the support surface.143−146  Using this method,   690

NiCa/Al2O3 was prepared and used as a catalyst for the CHC of 691

MSISPs from Runbei lignite and Shaerhu subtuminous coal at 692

180 °C.147 The yields of MSSPs from Runbei lignite and 693 Shaerhu subtuminous coal are 16.5% and 11.8%, respectively, 694 while those from the CHC under 1 MPa of IHP are 31.1% and 695 27.4%, respectively, i.e., the total yields of soluble portions by the 696

extraction and CHC are 47.6% and 39.2% based on the organic 697

Scheme 16. Possible Pathways for the Formation of H···H and H− and Subsequent H− Transfer to *C in 2-Phenoxy-1- phenylethanol to Induce 2-Phenoxy-1-phenylethanol  Depolymerization

J	https://doi.org/10.1021/acs.energyfuels.3c01713

Figure 3. A concept macromolecular network of typical heavy carbon resources.150

698 matters in Runbei  lignite  and  Shaerhu  subtuminous  coal, 699  respectively.  Interestingly,  only  alkanes  and  arenes  were 700 detected in the MSSPs from the CHC and their compositions 701 (in total 16 normal alkanes listed in Table S1, 5 branched alkanes

resources,  (2)  lack  of  deep  insight  into  the  features  of 736

macromolecular structures of the heavy carbon resources, and 737

(3) less attention paid to the mechanisms for the formation of 738

different active hydrogen species and their different roles in 739

702  listed  in  Table  S2,  and  47  arenes  listed  in  Table  S3)  are

directionally converting heavy carbon resources.

740

703 significantly simpler than those of coal tar and coal liquefaction

704 oil, not only enabling insight into the macromolecular structures 705 of the MSISPs but also facilitating the separation of the products. 706 ARs, including BR, NR, phenanthrene ring, anthracene ring, 707 pyrene ring, BR-BR, and BR-NR, in the precursors of the alkanes 708  and  arenes  could  be  connected  with  bridged  linkages   of

Although the macromolecular compositions of different heavy 741 carbon resources could be quite different, they have some similar 742 unit structures, i.e., ARs connected by bridged linkages and with 743 side chains on most of the ARs. Heteroatoms are contained in 744 some ARs, bridged linkages, and side chains, and numerous 745 soluble  organic  species  are  embedded  into  the  complex     746

709  −(CH2)m−O−(CH2)n− and/or side chains of  CH3(CH2)m−

macromolecular networks, as illustrated in Figure 3.149

747 f3

710  O−(CH2)n−. In NiCa/Al2O3, Ni activates H2  to H···H and Ca

711 splits H···H to mobile H− and immobile H+. H− transfer to the

712 oxygen atom in AR(CH2)m−O−(CH2)nAR and CH3(CH2)m− 713 O−(CH2)nAR and subsequent H+ abstraction from the surface 714 of H+-attached  NiCa/Al2O3  release  AR(CH2)m‑1CH3,  AR- 715 (CH2)n‑1CH3, and CH3(CH2)mCH3.  However,  at  180  °C 716 under 4 MPa of IHP, only alkanes and alkyl-substituted cyclanes 717 were detected in the products from the NiCa/Al2O3-catalyzed 718 hydroconversion of the MSISPs, indicating that H···H transfer 719 to  the  ARs  in  the  resulting  alkyl-substituted  moieties 720  predominantly proceeded.

721 Further  investigation  for  preparing  extremely  active  and 722 recyclable solid acids will facilitate cleaving most of the alkyl 723 groups on the ARs by effective H+ transfer to the ipso-positions 724  of  the  ARs  to  obtain  nonsubstituted  arenes,    especially

MS proved to be a powerful solvent for effectively extracting 748 the soluble organic species from the macromolecular networks 749 under ultrasonic irradiation.89,150,151 As a result, the organic 750 matter in heavy carbon resources can be isolated into soluble 751 portion and insoluble portion. A number of organic compounds 752

were significantly enriched and even separated as pure 753 compounds by subsequent fine separations, including fractional 754 extraction, gradient column chromatography, and sequential    755

crystallization from the soluble portion.152−159 Alternatively, the 756

soluble portion can be converted to alkanes as well as 757 nonsubstituted and alkyl-substituted cyclanes under pressurized 758 H2 over Ni-loading catalysts.57,58,88,135,160 The insoluble portion 759 can be ultrasonically isolated to a light insoluble portion and a 760 heavy insoluble portion in carbon tetrachloride according to the 761

86

725 nonsubstituted CAs, with significantly simpler    compositions

density difference.

The  catalytically  hydroconverted  light  762

726 for subsequent separation to obtain value-added pure arenes.

# CHALLENGES AND PERSPECTIVES

727 Developing smart technologies for the CHC of heavy carbon 728 resources to  value-added  products,  especially  condensed 729 aromatics and  cyclanes,5,81,148  under  mild  conditions  is  of 730 great importance for efficiently utilizing heavy carbon resources 731 to create great social wealth with near-zero emission of emission

732 of  exhaust  gas,  wastewater,  and  waste  residue.  The  key 733  challenges  facing  the  development  include:  (1)  the  high 734 contents of ARs and heteroatoms in addition to the insoluble 735 and complex macromolecular compositions of the heavy carbon

insoluble portion can be relatively easily separated from the 763

catalyst by the density difference, and adding a magnetic core 764 into the catalyst further facilitates recovering the cata- 765 lyst.83,119,131−135,161    In   addition,   ultrasonically   extracting   a 766

solid sample, e.g., a coal sample, significantly reduced the size 767 of the sample particles,150 facilitating the CHC. Using an 768 insoluble portion as the reactant makes an insight into the 769 mechanisms for the CHC easier by avoiding the disturbance of 770

the inherently existing soluble species in the raw sample. 771 Furthermore, removing soluble species from the raw sample also 772 makes the separation of a reaction mixture from the CHC easier. 773 Distinguishing the type of active hydrogen species is very 774 important for understanding the hydrogen transfer mechanism 775

K	https://doi.org/10.1021/acs.energyfuels.3c01713

Table 2. Roles of Catalysts in the Formation of Active Hydrogen Species and the Roles of the Resulting Active Hydrogen Species in the Hydroconversion of Organic Matter in

Typical Heavy Carbon Resources

ref.

9, 51−54, 68, 71, 72, 74, 75

61−67

78

71, 72, 74−78

cleaving some bridged linkages between ARs and side chains on ARs, and removing some heteroatoms

ditto

cleaving some bridged linkages between ARs and side chains on ARs, and leading to the satured hydrogenation of ARs and heteroatom removal

ditto

8, 81−86, 102, 108, 109, 112, 114,

116−119, 121, 129, 134

129−131, 134, 135

17, 57, 58, 87−91, 120, 140, 144

56, 128, 132, 133, 146

776 to provide scientific basis  for  constructing  a  highly active 777  catalyst.  Benzylic  hydrogen,  i.e.,  α-H,  is  easily  identified 778 according the sample structure. As mentioned above, catalytic 779 hydrogenation of 9,10-diphenylanthracene under  mild con- 780 ditions provides a proper evidence for H···H or H• transfer, since 781 H• transfer predominantly proceeds to 9- and 10-positions in 782 9,10-diphenylanthracene, while H···H transfer preferentially 783 occurs to other positions.71,72,77 According to the products from 784 the catalytic hydrocracking of benzyloxybenzene under mild 785 conditions, especially below 200 °C at which benzyloxybenzene 786 is inert toward thermolysis or by H• transfer, H+ transfer, and H− 787 transfer can be clearly  distinguished.  In  detail,  H+ transfer 788 predominantly proceeds to the oxygen atom in benzyloxyben- 789  zene  to  break  the  −O−CH2−  bond  and  yield  phenol and

790  toluene as the initial products162  because the oxygen atom    is

role of AH

cleaving bridged linkages in diarylmethanes and partially hydrogenating ARs ditto

ditto

791  most  negatively  charged141  and  the  resulting  tolylium   is 792 relatively stable, while H− transfer selectively occurs to the 793 ipso-carbon in the oxygen atom-connected BR of benzylox- 794 ybenzene to cleave the >Car−O− bond and generate benzene 795 and phenylmethanol as the initial products,130 due to the most 796 positive charged ipso-carbon.141

t2	797    As summarized in Table 2, both metal sulfides and carbon 798 materials can catalyze the formation of H•, but their catalyzes are 799 different. Over a metal sulfide, e.g., FeS2, H2 is converted to H• 800 via a chain reaction shown in Scheme 5, while H• results from

801 the homolytic splitting of H2 over a carbon material. H2 can be 802 activated to H···H over an ultrafine metal at temperatures lower 803 than 200 °C, but the resulting H···H can be easily split to H• at 804 temperatures higher than 300 °C. H• transfer to an ipso-position 805 in a diarylmethane induces the cleavage of AR-CH2AR bond due

806  to  the  formation  of  the  relatively  stable.CH2AR,  while H•

807  transfer  to  a  condensed  AR  only  leads  to  the     partial

AHa H• ditto ditto

H···H

hydrogenating ARs

H−

H···H and H+

H···H and H−

808 hydrogenation of the condensed AR, e.g., the  partial hydro- 809 genation of anthracene to 9,10-dihydroanthracene rather than 810 the saturated hydrogenation of anthracene to perhydroanthra- 811 cenes due to the low H•-accepting ability of the residual BRs in 812 9,10-dihydroanthracene and the stronger tendence for H•  to 813 abstract α-H from 9,10-dihydroanthracene.78 Solid acids and 814 solid bases tend to heterolytically split H2 to release H+ and H−, 815  respectively,  and  both  H+   and  H−   transfer  can  induce the

H+

activating H2 to H···H and heterolytically splitting H2 and H···H to release H+

activating H2 to H···H and heterolytically splitting H2

816 cleavage of bridged linkages between ARs and side chain on the 817 ARs, and the removal of some heteroatoms, but the positions 818  accepting H+  are quite different from those accepting H+     to

catalysis

a chain reaction shown in Scheme 5 homolytically splitting H2 homolytically splitting H···H

activating H2

heterolytically splitting H2  to release H+ heterolytically splitting H2  to release H−

s17	819  produce different products (Scheme 17). Both Ni/solid  acids 820 and Ni/solid bases have bifunctional catalyzes, i.e., Ni/solid 821 acids activates H2 to H···H and heterolytically splits H2 and H··· 822 H to release H+, while Ni/solid bases activates H2 to H···H and 823  heterolytically splits H2  and H···H to release H−. The synergic

824  transfer of either H···H and H+  or H···H and H−  leads to the

and H···H to release H−

825 effective cleavage of some bridged linkages between ARs and 826 some side chains on ARs, the saturated hydrogenation, and 827 heteroatom removal.

catalyst

metal sulfurs carbon materials ultrafine metals

(>300 °C)

ultrafine metals (<200 °C)

solid acids

solid bases Ni/solid acids

Ni/solid bases

aAH denotes active hydrogen.

828 Elaborately constructing highly active solid acids, solid bases, 829 Ni/solid acids, and Ni/solid bases is of great importance. Over 830 the catalysts, many bridged linkages and even some side chains 831 can be cleaved, and many heteroatoms outside and on ARs can 832 be removed by the CHC of light insoluble portions from heavy 833 carbon resources under mild conditions to get soluble portions 834 with relatively simple  composition,  facilitating  subsequent 835 separation to obtain  pure  chemicals,  especially value-added 836  chemicals,  such  as  condensed  aromatics.  The  remaining 837 economically inseparable species can be converted to  value- 838 added cyclanes by subsequent catalytic hydrofining.

L	https://doi.org/10.1021/acs.energyfuels.3c01713

Scheme 17. Difference between H+ Transfer and H− Transfer

# CONCLUSIONS

839 Directionally converting heavy carbon resources to more soluble 840 portion with simpler composition under mild conditions is a 841  crucial  step  for  efficiently  using  heavy  carbon   resources.

Feng-Yun Ma − Laboratory of Coal Clean Conversion & Chemical Engineering Process, College of Chemistry and Chemical Engineering, Xinjiang University, Urumqi 830046 Xinjiang Uyghur Autonomous Region, China

873

874

875

876

842  Compared to H•  transfer, the synergies between H+  and  H···

843 H transfer and between H− and H···H transfer are significantly

Zhi-Min Zong − Jiangsu Province Engineering Research Center 877

of Fine Utilization of Carbon Resources and Key Laboratory of 878

844 more effective for the process. Enhancing the synergies depends

Coal Processing and Efficient Utilization, Ministry of

879

845 on the construction of extremely active and recyclable catalysts,

846 over which  H2   can be  effectively  split  and/or  activated  to

Education, China University of Mining & Technology, Xuzhou 880

221116 Jiangsu, China;	orcid.org/0000-0002-3144-4558 881

847 produce high concentrations of H+ and H···H or H− and H···H

848 to directly crop the macromolecules in heavy carbon resources.

Wei Zhao − Jiangsu Province Engineering Research Center of

Fine Utilization of Carbon Resources and Key Laboratory of Coal Processing and Efficient Utilization, Ministry of

882

883

884

■

849	ASSOCIATED CONTENT

850  *sı     Supporting Information

851  The  Supporting  Information  is  available  free  of  charge at

Education, China University of Mining & Technology, Xuzhou 885 221116 Jiangsu, China;	orcid.org/0000-0002-5559-8957 886 Zhong-Hai Ni − Jiangsu Province Engineering Research Center 887 of Fine Utilization of Carbon Resources and Key Laboratory of 888

852      https://pubs.acs.org/doi/10.1021/acs.energyfuels.3c01713.

Coal Processing and Efficient Utilization, Ministry of

889

853	Tables of alkanes and arenes detected in SPsCHC  of  RL

854	and SSBC (PDF)

Education, China University of Mining & Technology, Xuzhou 890

221116 Jiangsu, China;	orcid.org/0000-0002-8706-2583 891

■

855	AUTHOR  INFORMATION

856  Corresponding Author

857	Xian-Yong Wei − Key Laboratory of Chemistry and Chemical

Xing Fan − Key Laboratory of Chemistry and Chemical

Engineering on Heavy-Carbon Resources, Yili Normal University, Yining 835000 Xinjiang, China;	orcid.org/ 0000-0001-5530-5563

Lin-Bing Sun − State Key Laboratory of Materials-Oriented

892

893

894

895

896

858	Engineering on Heavy-Carbon Resources, Yili Normal

Chemical Engineering, Jiangsu National Synergetic Innovation 897

859	University, Yining 835000 Xinjiang, China; Laboratory of 860	Coal Clean Conversion & Chemical Engineering Process, 861	College of Chemistry and Chemical Engineering, Xinjiang

Center for Advanced Materials, College of Chemical

Engineering, Nanjing Tech University, Nanjing 211816, China;	orcid.org/0000-0002-6395-312X

898

899

900

862	University, Urumqi 830046 Xinjiang Uyghur  Autonomous

Jing-Pei Cao − Jiangsu Province Engineering Research Center of 901

863	Region, China; Jiangsu Province Engineering Research Center

864	of Fine Utilization of Carbon Resources and Key Laboratory of

Fine Utilization of Carbon Resources and Key Laboratory of

Coal Processing and Efficient Utilization, Ministry of

902

903

865	Coal Processing and Efficient Utilization, Ministry of

866	Education, China University of Mining & Technology, Xuzhou

Education, China University of Mining & Technology, Xuzhou 904

221116 Jiangsu, China;	orcid.org/0000-0002-1544-7441 905

867	221116 Jiangsu, China;	orcid.org/0000-0001-7106-

868	4624; Email: wei_xianyong@163.com

Yun-Peng Zhao − Laboratory of Coal Clean Conversion &

Chemical Engineering Process, College of Chemistry and Chemical Engineering, Xinjiang University, Urumqi 830046

906

907

908

869 Authors

Xinjiang Uyghur Autonomous Region, China; Jiangsu Province 909

870	Xiang Bai − Key Laboratory of Chemistry and Chemical

Engineering Research Center of Fine Utilization of Carbon

910

871	Engineering on Heavy-Carbon Resources, Yili Normal

872	University, Yining 835000 Xinjiang, China

Resources and Key Laboratory of Coal Processing and Efficient 911

Utilization, Ministry of Education, China University of Mining 912

- https://doi.org/10.1021/acs.energyfuels.3c01713

| 913 | & Technology, Xuzhou 221116 Jiangsu, China; | orcid.org/ Xiang Bai received his Bachelor’s degree of science from Jingchu 974 |  |  |
| --- | --- | --- | --- | --- |
| 914 | 0000-0001-8120-0060 | University of Technology in 2013 and a Master’s degree of engineering 975 |  |  |
| 915 Shi-Chao Qi − State Key Laboratory of Materials-Oriented from Xinjiang University in 2016. He currently works at Yili Normal 976 |  |  |  |  |
| 916 | Chemical Engineering, Jiangsu National Synergetic Innovation |  | University and is studying for a Doctoral degree of science at Xinjiang | 977 |
| 917 | Center for Advanced Materials, College of Chemical |  | University with the major research interest of chemistry and chemical | 978 |
| 918 | Engineering, Nanjing Tech University, Nanjing 211816, |  | engineering of heavy carbon resources. | 979 |

919	China;   orcid.org/0000-0002-9609-7710

920 Jing Liang − Jiangsu Province Engineering Research Center of 921	Fine Utilization of Carbon Resources and Key Laboratory of 922	Coal Processing and Efficient Utilization, Ministry of

923	Education, China University of Mining & Technology, Xuzhou

924	221116 Jiangsu, China

925  Xiao-Ming Yue − Jiangsu Province Engineering Research Center

926	of Fine Utilization of Carbon Resources and Key Laboratory of

Feng-Yun Ma received her Bachelor’s degree of Engineering from East 980 China University of Science and Technology in 1982 and Master’s 981 degree of engineering from Dalian University of Technology in 2002. 982 She worked at Former Xinjiang Institute of Technology (now Xinjiang 983 University) as a Teaching Assistant during 1982-1987, Lecturer during 984 1988−1994, Associate Professor during 1994−1999, and Professor 985 during  1999−2020  with  the  major  research  interest  of  coal  clean 986

927	Coal Processing and Efficient Utilization, Ministry of

conversion and chemical engineering process.

987

928	Education, China University of Mining & Technology, Xuzhou

929	221116 Jiangsu, China

930	Fang-Jing Liu − Laboratory of Coal Clean Conversion &

931	Chemical Engineering Process, College of Chemistry and

932	Chemical Engineering, Xinjiang University, Urumqi 830046 933	Xinjiang Uyghur Autonomous Region, China; Jiangsu Province 934	Engineering Research Center of Fine Utilization of Carbon

Zhi-Min Zong received her Bachelor’s degree of science from Xuzhou 988 Normal College in 1982, a Master’s degree of engineering from The 989 University of Tokyo in 1992, and Doctoral degree of engineering from 990 China University of Mining & Technology in 1997. She worked at 991 China University of Mining & Technology as a Lecturer during 1993− 992 1998, Associate Professor during 1998−2002, and Professor during    993

2002−2020  with the  major  research interest  of  directional hydro-   994

935	Resources and Key Laboratory of Coal Processing and Efficient

936	Utilization, Ministry of Education, China University of Mining

conversion of heavy carbon resources.

995

937	& Technology, Xuzhou 221116 Jiangsu, China;	orcid.org/

938	0000-0003-3101-2090

939	Wen-Long Mo − Laboratory of Coal Clean Conversion & 940	Chemical Engineering Process, College of Chemistry and   941	Chemical Engineering, Xinjiang University, Urumqi 830046 942	Xinjiang Uyghur Autonomous Region, China;	orcid.org/

Wei Zhao received her Bachelor’s degree of science from Nanjing 996

University in 1988 and Master’s and Doctoral degrees of engineering 997 from China University of Mining & Technology (CUMT) in 2003 and 998 2009, respectively. She worked at CUMT as a Lecturer during 2000− 999 2003, Associate Professor during 2003−2011, and Professor from 2011 1000 with the major research interest of catalytic conversion of heavy carbon 1001

943	0000-0003-3837-0915

resources.

1002

944	Jing-Mei Liu − Laboratory of Coal Clean Conversion &

945	Chemical Engineering Process, College of Chemistry and   946	Chemical Engineering, Xinjiang University, Urumqi 830046 947	Xinjiang Uyghur Autonomous Region, China

948	Yu-Hong Kang − School of Chemistry and Chemical

949	Engineering, Yulin University, Yulin 719000 Shanxi, China

950	Guang-Hui Liu − School of Chemistry and Chemical

951	Engineering, Yulin University, Yulin 719000 Shanxi, China;

Zhong-Hai Ni received his Bachelor’s and Master’s degrees of 1003 engineering from China University of Mining and Technology 1004 (CUMT) in 2000 and 2003, respectively, and a Doctoral degree of 1005 science from Tsinghua University in 2006. He worked at Shandong 1006 University as a Lecturer during 2006-2008 and an Associate Professor 1007 in 2009 and at CUMT as a Professor from 2010 with the major research 1008 interest of chemistry and chemical engineering of coal tar-enriched 1009

952	orcid.org/0000-0003-0650-3875

condensed arenes.

1010

953	Zhong-Qiu Liu − Key Laboratory of Life-Organic Analysis of

954	Shandong Province, School of Chemistry and Chemical 955	Engineering, Qufu Normal University, Qufu 273165 956	Shandong, China

957	Li Li − Jiangsu Province Engineering Research Center of Fine

958	Utilization of Carbon Resources and Key Laboratory of Coal

Xing Fan received his Bachelor’s degree of science and Master’s degree 1011 of engineering from University of Science and Technology of China in 1012 2000 and 2004, respectively, and Doctoral degree of philosophy from 1013 Louisiana State University in 2010. He worked at Shandong University 1014 of Science and Technology as a Professor since 2019 with the major 1015 research interest of chemistry of heavy carbon resources. He is an 1016

959	Processing and Efficient Utilization, Ministry of Education,

960	China University of Mining & Technology, Xuzhou 221116

Emeritus Professor of Yili Normal University.

1017

961	Jiangsu, China

962  Complete contact information is available at:

963      https://pubs.acs.org/10.1021/acs.energyfuels.3c01713

964  Notes

965 The authors declare no competing financial interest.

Lin-Bing  Sun  received   his  Bachelor’s  and  Master’s  degrees  of    1018

engineering from China University of Mining & Technology in 2002 1019 and 2005, respectively. He received his Ph.D. from Nanjing University 1020 in 2008. Then, he joined Nanjing Tech University and is a Professor of 1021 the university with current research interests focusing on fabrication of 1022 porous functional materials and their applications in adsorption and 1023 catalysis. He was a postdoctoral research associate at Texas A&M 1024

966 Biographies

University in 2011−2012.

1025

967 Xian-Yong Wei received his Bachelor’s degree of science from Nanjing 968  University  in  1982  and  his  Master’s  and  Doctoral  degrees  of 969 engineering from  The  University  of  Tokyo  in  1989  and  1992, 970 respectively. He worked at China University of Mining & Technology 971 as a professor from 1993 to 2023 with the major research interest of 972  chemistry and chemical engineering of heavy carbon resources.    He

Jing-Pei Cao received his Bachelor’s degree of science and Master’s 1026 degree of engineering from China University of Mining and 1027 Technology (CUMT) in 2004 and 2007, respectively, and a Doctoral 1028 degree of engineering from Gunma University in 2011. He worked at 1029 CUMT as an Associate Professor during 2012−2015 and a Professor 1030 since 2016. His research interest is value-added utilization of coals and 1031

973 currently works at Yili Normal University as an emeritus professor.

biomass.

1032

- https://doi.org/10.1021/acs.energyfuels.3c01713

1033  Yun-Peng Zhao received his Bachelor’s degree of engineering   from

from 2023 with the major research interest of efficient utilization of   1093

1034 Zhengzhou University in 2005 and Doctoral degree of engineering from

heavy carbon resources.

1094

1035 Dalian University of Technology  in  2010.  He  worked  at  China 1036 University of Mining & Technology as a Lecturer during 2011−2014 1037 and Associate Professor during 2014−2021, and has been working at 1038 the university as a Professor from 2021. His major research interests are 1039 thermal conversion of coals and biomass.

1040 Shi-Chao Qi received his Bachelor’s degree of science from China

Zhong-Qiu Liu received his Bachelor’s degree of science from Jining 1095 University in 2011, Master’s degree of engineering from Jiangsu Normal 1096 University in 2014, and Doctoral degree of engineering from China 1097 University of Mining & Technology in 2018. He worked at Qufu 1098 Normal University as a Lecturer during 2018−2022 and an Associate 1099 Professor since 2022 with the major research interest of directional    1100

1041 University of Petroleum in 2011, Master’s degree of engineering from

hydroconversion of heavy carbon resources.

1101

1042 China University of Mining & Technology in 2014, and Doctoral 1043 degree of engineering from Kyushu University in 2017. Then he joined 1044 Nanjing Tech University as a lecturer has been working at the university

Li Li received her bachelor of Science in 2010, Master’s degree of 1102

engineering in 2013, and Doctoral degree of engineering in 2023 from 1103

China University of Mining & Technology. Her major research focuses 1104

1045 as an Associate Professor from 2020. His current research area is

1046 advanced porous materials, heterogeneous catalysis, quantum chemical

1047  calculation, and molecular simulation.

1048 Jing Liang received her Bachelor’s and Master’s degrees of science from

on directional hydroconversion of heavy carbon resources.

# ACKNOWLEDGMENTS

1105

1106

1049 Soochow University in 1996 and 1999, respectively, and Doctoral 1050 degree of engineering from China University of Mining & Technology 1051 (CUMT) in 2015. She worked at Xuzhou Medical University as a 1052 lecturer during 2000−2004, at CUMT as a Lecturer during 2004−2008 1053 and an Associate Professor from 2009. Her current research area is 1054 green organic synthesis and catalytic  conversion  of  heavy carbon 1055 resources.

Our related work was subsidized by the National Basic Research 1107

Program of China (Grants 2004CB217801, 2004CB217601, 1108 2007CB210205, and 2011CB201302), the National Natural 1109 Science  Foundation  of  China  (Grants 29676045,  20076051, 1110

90410018,   20676142,   20776149,   20936007,   50921002, 1111

51221462,   51074153,   51134021,   21206187,   21206188, 1112

U1503293,  21676292,  21776298,  and  U1710102),  and  the  1113

National Natural Science Foundation of Yili Normal University 1114

1056  Xiao-Ming  Yue  received  her  Bachelor’s  and  Doctoral  degrees of

1057 engineering from China University of Mining & Technology (CUMT) 1058 in 2007 and 2012, respectively. She worked at CUMT as a Lecturer 1059 during 2012−2016 and an Associate Professor from 2017 with current

(Grant 22XKZY07).

# ABBREVIATIONS USED

1115

1116

1060  interests  focusing  on  advanced  porous  materials  and    catalytic

1061 conversion of coals.

1062 Fang-Jing Liu received his Bachelor’s degree of science and Master’s 1063 and Doctoral degrees of engineering from China University of Mining 1064 & Technology (CUMT) in 2009, 2012, and 2016, respectively. Then 1065 he worked at University of Wyoming as a postdoc associate scientist. He

1066 joined CUMT as a Lecturer and worked at CUMT as an Associate

ARs,  aromatic  rings;   BR,   benzene  ring;   CHC,   catalytic 1117

hydroconversion; COBBs, C−O bridged bonds; DPMG, 1118 diphenylmethyl group; IHP, initial hydrogen pressure; MS, 1119 isometric carbon disulfide/acetone mixed solvent; MSISP, MS- 1120 insoluble portion; MSSP, MS-soluble portion; LRMCs, lignin- 1121 related model compounds; MMG, macromolecular group; 1122 MMGSAR, MMG-substituted anthracene ring; NCHC, non-   1123

1067 Professor from 2020. His current research area is coal structure and coal

1068 directional conversion to valued-added chemicals.

1069  Wen-Long  Mo  received  his  bachelor  and  doctoral  degrees      of

catalytic hydroconversion; NR, naphthalene ring

# REFERENCES

1124

1125

1070  engineering from Xinjiang University in 2011 and 2016, respectively.

- Wei, X. Y.; Zong, Z. M.; Sun, L. B.; Qin, Z. H.; Zhao, W. Scientific 1126

foundation for efficient utilization of heavy carbon resources. Chem. Ind. 1127

1071 He worked at Xinjiang University as a Lecturer during 2016−2017 and

Eng. Pro. 2006, 25, 1134−1142.

1128

1072 Associate Professor from 2018 with the major research interest of

1073  heterogeneous  catalysis,  advanced  porous  materials,  and chemical

- Wei, X. Y. Technological innovation for efficient utilization of 1129

heavy carbon resources, 2020 Int. Forum Petrochem. Green Dev. October 1130

1074 engineering of heavy carbon resources.

18 & 19, 2020, Xuzhou, China.

1131

1075  Jing-Mei  Liu  received  bachelor,  master,  and  doctoral  degrees  of

1076  engineering  from  Xinjiang  University  in  2006,  2009,  and    2019,

- Wei, X. Y. Technology development for efficient utilization of 1132

heavy carbon resources, 2020 Int. Forum Petrochem. Green Dev. April 17, 1133

2020, Shanghai, China.

1134

1077  respectively.  She  worked  at  Xinjiang  University  as  a      assistant

1078 experimentalist during 2009-2013, experimentalist during 2014-2019, 1079 and senior experimentalist since 2020 with the major research interest 1080 of clean conversion of coals.

- Wei, X. Y.; Zong, Z. M.; Zhao, W.; Ni, Z. H.; Cao, J. P.; Fan, X.; 1135 Zhao, Y. P.; Zhao, X. Y.; Liang, J.; Liu, F. J.; Kang, Y. H.; Ma, F. Y.; 1136 Aisha, N.; Mo, W. L.; Liu, J. M. Chemical technology development for 1137 efficient utilization of heavy carbon resources, The 2nd Int. Conf. Appl. 1138

1081  Yu-Hong Kang received his Bachelor’s degree of engineering    from

Chem. Ind. Catal., October 16−19, 2020, Dalian, China.

1139

1082  Henan  University  in  2007,  Master’s  degree  of  engineering  from

- Wei, X. Y.; Zong, Z. M.; Fan, X.; Li, Z. K. Chapter 17. Coal-based 1140

products and their uses. In: Coal Production and Processing Technology. 1141

1083  Taiyuan University of Technology in 2012, and Doctoral degree    of

CRC Press: 2015; pp  383−412.

1142

1084  engineering from China University of Mining & Technology in 2021.

1085  He worked at Yulin University as a Teaching Assistant during 2012−

1086 2014, Lecturer during 2014−2018, and Associate Professor since 2018

- Sun, L. B.; Zong, Z. M.; Kou, J. H.; Cao, J. P.; Yu, G. Y.; Zhao, W.; 1143 Li, B. M.; Lee, C. W.; Xie, K. C.; Wei, X. Y. Identification of organic 1144 chlorines and iodines in the extracts from hydrotreated Argonne 1145

1087 with the major research interest of chemical engineering of heavy

Premium coal residues. Energy Fuels 2007, 21, 2238−2239.

1146

1088 carbon resources.

1089  Guang-Hui Liu received his Bachelor’s degree of engineering    from

- Sun, L. B.; Wei, X. Y.; Liu, X. Q.; Zong, Z. M.; Li, W. Release of 1147

organonitrogen and organosulfur compounds during hydrotreatment 1148

of Pocahontas No. 3 coal residue over an activated carbon. Energy Fuels 1149

1090  Tongji University in 2014 and doctoral degree of engineering    from

2009, 23, 5284−5286.

1150

1091  China University of Mining & Technology in 2020. Then he    joined

1092 Yulin University, where he has been working as an Associate Professor

- Xiao-Ming, Y.; Xian-Yong, W.; Bing, S.; Ying-Hua, W.; Zhi-Min, 1151

Z.;  Zi-Wu,  L.  Solid  superacid-catalyzed  hydroconversion  of  an   1152

- https://doi.org/10.1021/acs.energyfuels.3c01713

1153 extraction residue from Lingwu bituminous coal. Int. J. Mining   Sci.

(29)

Yang,   X.;  Shao,  S.;   Li,  X.;  Tang,   D.  Catalytic  transfer   1220

1154 Technol. 2012, 22, 251−254.

hydrogenation  of  bio-oil  over  biochar-based  CuO  catalyst  using  1221

1155

- Yu, L. C.; Wei, X. Y.; Wang, Y. H.; Zhang, D. D.; Wen, Z.; Zong, Z.

methanol as hydrogen donor. Renew. Energy 2023, 211, 21−30.

1222

1156 M.; Fan, X.; Zhao, Y. P.; Zhao, W.; Zhu, Y. L. Catalytic hydroconversion 1157 of extraction residue from Shengli lignite over Fe-S/ZSM-5. Fuel 1158 Process. Technol. 2014, 126, 131−137.

(30) Ai, L.; Shi, H.; Chen, J. In-situ deoxygenation of methyl palmitate 1223

to hydrocarbons on highly dispersed Ni−Re/TiO2 catalyst in aqueous 1224

phase using methanol as a hydrogen donor. J. Energy Inst. 2023, 109, 1225

1159

- Kuhlmann, E. J.; Jung, D. Y.; Guptill, R. P.; Dyke, C. A.; Zang, H.

101265.

1226

1160 K. Coal liquefaction using a hydrogenated creosote oil solvent: H-atom 1161 transfer from hydrogen donor components in the solvent. Fuel 1985, 1162  64, 1552−1557.

(31) Lu, H. Y.; Wei, X. Y.; Yu, R.; Peng, Y. L.; Qi, X. Z.; Qie, L. M.; 1227

Wei, Q.; Lv, J.; Zong, Z. M.; Zhao, W.; Zhao, Y. P.; Ni, Z. H.; Wu, L. 1228

Sequential thermal dissolution of Huolinguole lignite in methanol and 1229

1163

- Bate, K.; Harrison, G. Fate of hydrogen-donor molecules in two-

in ethanol. Energy Fuels 2011, 25, 2741−2745.

1230

1164 stage liquefaction using model solvents. Fuel 1992, 71, 289−293.

(32) Chen, B.; Wei, X. Y.; Zong, Z. M.; Yang, Z. S.; Qing, Y.; Liu, C. 1231

1165

(12) Sudakova, I. G. Influence of hydrogen donor solvent on kinetic

Difference in chemical composition of the products from supercritical 1232

1166 features of hydrogenation of some fluid products of coal liquefaction.

methanolysis of two lignites. Appl. Energy 2011, 88, 4570−4576.

1233

1167 Coal Sci. Technol. 1995, 24, 1491−1494.

(33) Chen, B.; Wei, X. Y.; Yang, Z. S.; Liu, C.; Fan, X.; Qing, Y.; Zong, 1234

1168

- Liu, J.; Zhao, L.; Liu, Z.; Liu, Q. Catalyst-free liquefaction of

Z. M. ReaxFF reactive force field for molecular dynamics simulations of 1235

1169 lignin for monophenols in hydrogen donor solvents. Fuel    Process.

lignite depolymerization in supercritical methanol with lignite-related  1236

1170 Technol. 2022, 229, 107180.

model compounds. Energy Fuels 2012, 26, 984−989.

1237

1171

- Shimada, I.; Uno, C.; Watanabe, Y.; Takatsuka, T. Catalytic

(34) Li, Z. K.; Zong, Z. M.; Yan, H. L.; Wang, Y. G.; Wei, X. Y.; Shi, D. 1238

1172 cracking of three-ring polycyclic aromatic hydrocarbons in the presence

1173 of hydrogen donors. Fuel Process. Technol. 2022, 232, 107267.

L.; Zhao, Y. P.; Zhao, C. L.; Yang, Z. S.; Fan, X. Alkanolysis simulation 1239

of lignite-related model compounds using density functional theory.   1240

1174

- Liu, M.; Yang, J.; Li, Y.; Liu, Z.; Liu, Q.; Shi, L. Radical reactions

Fuel 2014, 120, 158−162.

1241

1175  and two-step kinetics of sub-bituminous coal liquefaction in  various

1176 solvents. Energy Fuels 2019, 33 (3), 2090−2098.

(35) Li, Z. K.; Zong, Z. M.; Yan, H. L.; Wang, Y. G.; Ni, H. X.; Wei, X. 1242

Y.; Li, Y. H. Characterization of acidic species in ethanol-soluble 1243

1177

- Sheng, Q.; Wang, G.; Zhang, Q.; Gao, C.; Ren, A.; Duan, M.;

portion from Zhaotong lignite ethanolysis by negative-ion electrospray 1244

1178  Gao, J. Seven-lump kinetic model for non-catalytic hydrogenation of

ionization Fourier transform ion cyclotron resonance mass spectrom- 1245

1179 asphaltene. Energy Fuels 2017, 31 (5), 5037−5045.

etry. Fuel Process. Technol. 2014, 128, 297−302.

1246

1180

- Yung, M. M.; Starace, A. K.; Mukarakate, C.; Crow, A. M.;

(36) Yang, H. M.; Zhao, W.; Norinaga, K.; Fang, J. J.; Wang, Y. G.;  1247

1181 Leshnov, M. A.; Magrini, K. A. Biomass catalytic pyrolysis on Ni/ZSM-

1182 5: Effects of nickel pretreatment and loading. Energy Fuels 2016, 30 (7),

Zong, Z. M.; Wei, X. Y. Separation of phenols and ketones from bio-oil 1248

produced from ethanolysis of wheat stalk. Sep. Purif. Technol. 2015, 152, 1249

1183  5259−5268.

238−245.

1250

1184

(18)  Zong,  Z.  M.;  Zhang,  W.  H.;  Jiang,  Q.;  Lu,  J.;  Wei,  X. Y.

(37) Liu, F. J.; Wei, X. Y.; Zong, Z. M.; Fan, M. H. Characterization of 1251

1185  Photochemical reactions of hydroarenes with  N-bromosuccinimide.

the oxygenated chemicals produced from supercritical methanolysis of 1252

1186 Bull. Chem. Soc. Jpn. 2002, 75, 769−771.

modified lignites. Energy Fuels 2016, 30, 2636−2645.

1253

1187

(19) McMillen, D. F.; Malhotra, R.; Nigenda, S. E. The case for

(38) Yan, H. L.; Zong, Z. M.; Li, Z. K.; Kong, J.; Zheng, Q. X.; Zhao, 1254

1188 induced bond scission during coal pyrolysis. Fuel 1989, 68, 380−386.

M. X.; Li, Y.; Wei, X. Y. Insight into the chemical complexity of soluble 1255

1189

(20) Zong, Z. M.; Wei, X. Y. Effects of molecular hydrogen and

portions from cornstalk methanolysis. Energy Fuels 2016, 30, 3020− 1256

1190  hydrogen donor additives on 1,2-di(1-naphthyl)ethane    thermolysis.

3029.

1257

1191 Fuel Process. Technol. 1994, 41, 79−85.

(39) Hu, L.; Guo, X. H.; Wei, X. Y.; Liu, F. J.; Xu, M. L.; Liu, T. L.;  1258

1192

- Wei, X. Y.; Ogata, E.; Zong, Z. M.; Niki, E. Inhibiting effect of

Zhang, F. B. Research on the influence of sequential isopropanolysis  1259

1193 hydrogen-donating compounds on1,3-diphenylpropane. Coal  Conv.

liquefaction on the composition of liquid tars and physicochemical 1260

1194  1995, 18, 67−70.

structure evolution of renbei lignite. Energy 2023, 279, 128097.

1261

1195

- McMillen, D. F.; Malhotra, R.; Chang, S. J.; Ogier, W. C.;

(40) Bai, Y.; Cui, K.; Sang, Y.; Wu, K.; Yan, F.; Mai, F.; Ma, Z.; Wen, 1262

1196  Nigenda, S. C.; Fleming, R. H. Mechanisms of hydrogen transfer and

1197 bond scission of strongly bonded coal structures in donor-solvent

Z.; Chen, H.; Chen, M.; Li, Y. Catalytic Depolymerization of a lignin- 1263

rich corncob residue into aromatics in supercritical ethanol over an    1264

alumina-supported NiMo alloy catalyst. Energy Fuels 2019, 33 (9),   1265

1198 systems. Fuel 1987, 66, 1611−1620.

8657−8665.

1266

1199

(23) Futamura, S.; Koyanagi, S.; Kamiya, Y. The hydrogenolysis   of

- Li, C.; Zhang, M.; Li, H.; Zhang, Y. Renewable tar-derived Pd@ 1267

1200  diarylmethane. Mechanism for hydrogen transfer from solvents  and

biocarbon for mild and efficient selectively hydrodeoxygenation of 1268

1201 additive effects of hydrogen shuttlers and organic radical sources. Fuel

vanillin. Energy Fuels 2021, 35 (5), 4169−4181.

1269

1202  1988, 67, 1436−1440.

- Curran, G. P.; Struck, R. T.; Gorin, E. Mechanism of hydrogen- 1270

1203

(24) Hu,  J.;  Zhao, M.;  Jiang,  B.;  Wu, S.; Lu, P.  Catalytic  transfer

transfer process to coal and coal extract. Ind. Eng. Chem. Process. Des. 1271

1204  hydrogenolysis of native lignin to monomeric phenols over a Ni−Pd

Dev. 1967, 6, 166−173.

1272

1205 bimetallic catalyst. Energy Fuels 2020, 34 (8), 9754−9762.

(43) Kamiya, Y.; Nagae, S. Relative reactivity of hydrogen donor 1273

1206

(25) Song, L.; Ouyang, Y.; Huang, S.; Li, Z.; Sun, M. Insight into

solvent in coal liquefaction. Fuel 1985, 64, 1242−1245.

1274

1207 liquefaction process of sawdust with hydrogen donor solvents. Biomass

(44) Chiba, K.; Tagaya, H.; Saito, N. Liquefaction of Yallourn coal by 1275

1208 Bioenerg. 2022, 160, 106444.

binary system solvent. Energy Fuels 1987, 1, 338−343.

1276

1209

(26) Zhang, J.; Li, C.; Hu, S.; Gu, J.; Yuan, H.; Chen, Y. Mechanistic

(45)

Woodfine,  B.;  Steedman,  W.;  Kemp,  W.  Donor  solvent   1277

1210 insights into copper oxides catalyzed bio-based furfural hydrogenation

interactions during coal liquefaction. Fuel 1989, 68, 293−297.

1278

1211 using methanol as in-situ hydrogen donor. Renew. Energy 2022, 200,

- Bate, K.; Harrison, G. Fate of hydrogen-donor molecules in two- 1279

1212  88−97.

stage liquefaction using model solvents. Fuel 1992, 71, 289−293.

1280

1213

(27)

Mu,  D.;  Li,  Z.;  Yu,  S.;  Liu,  S.  Hydrodechlorination     of

- Park, H. B.; Kim, K. D.; Lee, Y. K. Promoting asphaltene 1281

1214 chlorophenols with methanol as hydrogen donor over carbon nanotube

conversion by tetralin for hydrocracking of petroleum pitch. Fuel 2018, 1282

1215 supported Pd-catalysts. Catal. Today 2022, 405−406, 47−56.

222, 105−113.

1283

1216

(28)

Philippov,  A.  A.;  Anufrieva,  V.  M.;  Pakharukova,  V.   P.;

- Miura, K.; Shimada, M.; Mae, K.; Sock, H. Y. Extraction of coal 1284

1217  Martyanov, O. N.  Donor activity of sub-  and supercritical   primary

1218 alcohols  in  catalyst-free  and  Ni/γ-Al2O3   catalyzed  transfer hydro-

below 350 °C in flowing non-polar solvent. Fuel 2001, 80, 1573−1582. 1285

- Ouchi, K.; Makabe, M. Hydrogen transfer in the hydrogenation 1286

1219 genation of furfural. J. Supercrit. Fluid 2023, 193, 105815.

of model compounds. Fuel 1988, 67, 1536−1541.

1287

- https://doi.org/10.1021/acs.energyfuels.3c01713

1288

- Niu, B.; Jin, L. J.; Li, Y.; Shi, Z. W.; Li, Y. T.; Hu, H. Q.

- Herndon, W. C. Resonance energies of hydrocarbon radicals. 1356

1289 Mechanism of hydrogen transfer and role of solvent during heating-up

radical reactivities of polycyclic aromatic hydrocarbons. J. Org. Chem. 1357

1290 stage of direct coal liquefaction. Fuel Process. Technol. 2017, 160, 130−

1981, 46, 2119−2125.

1358

1291  135.

- Zhou, S. L.; Ni, Z. H.; Yuan, X. H.; Zong, Z. M.; Wei, X. Y. 1359

1292

- Wei, X. Y.; Ogata, E.; Niki, E. FeS2-catalyzed hydrocracking of

Catalyses of metals and their sulfides in selective hydrogenation of 9,10- 1360

1293 di(1-naphthyl)methane. Bull. Chem. Soc. Jpn. 1992, 65, 987−990.

diphenylanthracene. J. China Univ. Mining Technol. 2001, 11, 80−82.

1361

1294

- Wei, X. Y.; Ogata, E.; Niki, E. FeS2-catalyzed hydrocracking of

(72) Zhou, S. L.; Ni, Z. H.; Yuan, X. H.; Zong, Z. M.; Wei, X. Y. Study 1362

1295 diarylmethanes. Sekiyu Gakkaishi 1992, 35, 358−361.

on the mechanism of catalytic hydrogenation of 9,10-diphenylan- 1363

1296

(53) Wei, X. Y.; Zong, Z. M. Solvent effect on diphenylmethane

thracene by GC-MS. J. Fuel Chem. Technol. 2001, 29, 80−82.

1364

1297 hydrocracking. Energy Fuels 1992, 6, 236−237.

(73) Wei, X. Y.; Zong, Z. M.; Zhao, W.; Cao, J. P.; Liu, Z. W.; Fan, X.; 1365

1298

- Wei, X. Y.; Ogata, E.; Zong, Z. M.; Niki, E. Effects of iron catalyst

Zhao, Y. P.; Zhao, X. Y. Directional conversion of coals: challenges and 1366

1299  precursors,  sulfur,  hydrogen  pressure  and  solvent  type  on     the

prospects. 2017 Int. Conf. Coal Sci. Technol. & 2017 Australia-China 1367

1300 hydrocracking of di(1-naphthyl)methane. Fuel 1993, 72, 1547−1552.

Symp. Energy, September 25−29, 2017, Beijing, China, No. O5−4,.

1368

1301

- Li, Z. K.; Wei, X. Y.; Yan, H. L.; Yu, X. Y.; Zong, Z. M.

- Wei, X. Y.; Ogata, E.; Niki, E. Catalyses of Fe and FeS2 on the 1369

1302  Characterization  of  soluble  portions  from  thermal  dissolution of

1303 Zhaotong lignite in cyclohexane and methanol. Fuel Process. Technol.

1304  2016, 151, 131−138.

reaction of di(1-naphthyl)-methane. Chem. Lett. 1991, 20, 2199−2202. 1370

- Wei, X. Y.; Ni, Z. H.; Zong, Z. M.; Zhou, S. L.; Xiong, Y. C.; 1371

Wang, X. H. Reaction of di(1-naphthyl)methane over metals and metal- 1372

1305

- Li, X. K.; Zong, Z. M.; Chen, Y. F.; Yang, Z.; Liu, G. H.; Liu, F. J.;

sulfur systems. Energy Fuels 2003, 17, 652−657.

1373

1306 Wei, X. Y.; Wang, B. J.; Ma, F. Y.; Liu, J. M. Catalytic hydroconversion

1307 of Yinggemajianfeng lignite over difunctional Ni-Mg2Si/γ-Al2O3. Fuel

(76) Qi, S. C.; Wei, X. Y.; Zong, Z. M.; Hayashi, J. I.; Yuan, X. H.; Sun, 1374

L. B. A highly active Ni/ZSM-5 catalyst for complete hydrogenation of 1375

1308  2019, 249, 496−502.

polymethylbenzenes. ChemCatChem. 2013, 5,  3543−3547.

1376

1309

- Kang, Y. H.; Wei, X. Y.; Liu, G. H.; Ma, X. R.; Gao, Y.; Li, X.; Li, Y.

- Qi, S. C.; Wei, X. Y.; Hayashi, J. I.; Zong, Z. M.; Guo, L. L.; et al. 1377

1310 J.; Ma, Y. J.; Yan, L.; Zong, Z. M. Catalytic hydroconversion of ethanol-

Deep hydrogenation of coal tar over Ni/ZSM-5 catalyst. RSC Adv.    1378

1311 soluble portion from the ethanolysis of Hecaogou subbituminous coal

2014, 4, 17105−17109.

1379

1312 extraction residue to clean liquid fuel over a Y/ZSM-5 composite

1313 zeolite-supported nickel catalyst. Energy Fuels 2020, 34, 4799−4807.

- Liu, Z. Q.; Wei, X. Y.; Liu, F. J.; Wang, B. J.; Zong, Z. M. 1380

Temperature-controlled  hydrogenation  of  anthracene  over  nickel  1381

1314

- Kang, Y. H.; Wei, X. Y.; Liu, G. H.; Gao, Y.; Li, Y. J.; Ma, X. R.;

nanoparticles supported on attapulgite powder. Fuel 2018, 223, 222− 1382

1315 Zhang, Z. F.; Zong, Z. M. Catalytic hydroconversion of soluble portion

1316 in the extraction from Hecaogou subbituminous coal to clean liquid fuel

229.

(79)

1383

Wei,  X.  Y.  Chemical  basis  for  the  directional  catalytic 1384

1317 over a Y/ZSM-5 composite zeolite-supported nickel catalyst. Fuel 2020,

hydroconversion of heavy carbon resources. The First Forum on Green 1385

1318  269, 117326.

Chemical Technology Development; Shanghai, China, 2019.

1386

1319

- Kang, Y. H.; Ma, Z. Y.; Zhang, X. Q.; Wei, X. Y.; Li, Y. J.; Liu, G.

- Reed, C. A.; Kim, K. C.; Bolskar, R. D.; Mueller, L. J. Taming 1387

+	.+

1320  H.;  Wang,  A.  M.;  Ma,  X.  R.;  Yan,  L.;  Zong,  Z.  M.;  Bai,  H. C.

superacids: stabilization of the fullerene cations HC60  and C60  . Science 1388

1321  Investigation on the structural features of Hecaogou  subbituminous

2000, 289, 101−104.

1389

1322 coal and its residues by multiple technical strategies. Fuel 2022, 309,

1323  122111.

- Wei, X Y. Catalytic hydroconversion of low-rank coals under 1390

mild conditions and the synthesis of CO2-based polymers. The 358th 1391

1324

- Li, L.; Wei, X. Y.; Shao, C. W.; Yin, F.; Sun, B. K.; Liu, F. J.; Li, J.

symposium on Green and Low Carbon Development of Coal Engineering 1392

1325  H.;  Liu,  Z.  Q.;  Zong,  Z.  M.  Honeycomb-like  N/O   self-doped

Science and Technology, Chinese Acadymy of Engineering & Summit of the 1393

1326  hierarchical  porous  carbons  derived  from  low-rank  coal  and  its

6th Coal Science and Technology; Beijing, China, 2023.

1394

1327 derivatives for high-performance supercapacitor. Fuel 2023,     331,

1328  125658.

(82) Yue, X. M.; Wei, X. Y.; Sun, B.; Wang, Y. H.; Zong, Z. M.; Fan, X.; 1395

Liu, Z. W. A new solid acid for specifically cleaving the Car-Calk bond in 1396

1329

- Ni, Z. H.; Zong, Z. M.; Zhang, L. F.; Sun, L. B.; Liu, Y.; Yuan, X.

di(1-naphthyl)methane. Appl. Catal. A Gen. 2012, 425−426, 79−84.

1397

1330  H.; Wei, X. Y. Synergic effect of sulfur on activated carbon-catalyzed

1331 hydrocracking of di(1-naphthyl)methane. Energy Fuels 2003, 17, 60−

1332 61.

(83) Yang, Z.; Wei, X. Y.; Zhang, M.; Teng, D. G.; Wang, Y. N.; Liu, Z. 1398

Q.; Zong, Z. M. Enhanced hydrocracking Car-Calk bridged bonds in the 1399

extraction residue from Piliqing subbituminous coal over a recyclable 1400

1333

- Sun, L. B.; Zong, Z. M.; Kou, J. H.; Zhang, L. F.; Ni, Z. H.; Yu, G.

and active magnetic solid superacid. Fuel Process. Technol. 2018, 176, 1401

1334 Y.;  Chen,  H.;  Wei,  X.  Y.;  Lee,  C.  W.  Activated carbon-catalyzed

316−324.

1402

1335 hydrogenation of polycylic arenes. Energy Fuels 2004, 18, 1500−1504.

(84) Yang, Z.; Wei, X. Y.; Li, Z. X.; Zhang, M.; Zong, Z. M.; Wei, Z. H.; 1403

1336

- Sun, L. B.; Zong, Z. M.; Kou, J. H.; Liu, G. F.; Sun, X.; Wei, X. Y.;

Li,  Y.  MOFs-derived  N-doped  carbon  matrix  superacid-catalyzed 1404

1337 Zhou, G. J.; Lee, C. W. Activated carbon-catalyzed hydrogen transfer to

hydrocracking  of  a  residue  from  thermal  dissolution  of  Hefeng  1405

1338  α,ω-diarylalkanes. Energy Fuels 2005, 19, 1−6.

subbituminous coal. Fuel Process. Technol. 2018, 180, 180−188.

1406

1339

- Sun, L. B.; Wei, X. Y.; Liu, X. Q.; Zong, Z. M.; Li, W.; Kou, J. H.

- Zhao, M. X.; Yang, N.; Xie, H. S.; Zhao, Z.; Zong, Z. M.; Wei, X. 1407

1340  Selective hydrogen transfer to anthracene and its derivatives over  an

Y. Catalytic hydroconversion of extraction residues from two Chinese 1408

1341 activated carbon. Energy Fuels 2009, 23, 4877−4882.

coals to arenes. Fuel 2021, 284, 118910.

1409

1342

(65)

Farcasiu,  M.;   Smith,  C.   Modeling  coal  liquefaction.   1.

- Wu, Z. F.; Wei, X. Y.; Mo, W. L.; Kang, Y. H.; Zhang, X. Q.; Shan, 1410

1343  decomposition of 4-(1-naphthylmethyl)bibenzyl catalyzed by  carbon

1344 black. Energy Fuels 1991, 5, 83−87.

X. K.; Liu, G. H.; Fan, X. Catalytic hydroconversion of the light residue 1411

from Yinggemajianfeng lignite over a solid superacid. Fuel 2022, 310, 1412

1345

- Farcasiu, M.; Petrosius, S. C.; Eldredge, P. A.; Anderson, R. R.;

122470.

1413

1346 Ladner, E. P. Modeling coal liquefaction. 3. catalytic reactions of

1347 polyfunctional compounds. Energy Fuels 1994, 8, 920−924.

(87) Zhou, X.; Wei, X. Y.; Ma, Y. M.; Zong, Z. M. Highly selective   1414

catalytic hydrocracking C-O bridged bonds in an alkali lignin over Ni/ 1415

1348

- Farcasiu, M.; Kaufman, P. B.; Ladner, E. P.; Derbyshire, F.;

Hβ. Fuel 2021, 287, 119474.

1416

1349 Jagtoyen, M. Carbon catalysts for reactions relevant to coal liquefaction.

1350 Proc. Int. Conf. Coal Sci. 1995, 24, 1303−1306.

(88) Li, W. T.; Wei, X. Y.; Liu, X. X.; Guo, L. L.; Qi, S. C.; Li, Z. K.; 1417

Zhang, D. D.; Zong, Z. M. Catalytic hydroconversion of methanol-   1418

1351

- Wei, X. Y.; Ogata, E.; Niki, E. FeS2-catalyzed hydrocracking of

soluble portion from Xiaolongtan lignite over difunctional Ni/Z5A.   1419

1352 α,ω-diarylalkanes. Bull. Chem. Soc. Jpn. 1992, 65, 1114−1119.

Fuel Process. Technol. 2016, 148, 146−154.

1420

1353

- Yonezawa, T.; Nagata, C.; Kato, H.; Imamura, A.; Morokuma, K.

- Kang, Y. H.; Wei, X. Y.; Li, J.; Jin, H. T.; Li, T.; Lu, C. Y.; Ma, X. 1421

1354 Guide to Quantum Chemistry; Kagaku-Dojin Press: Kyoto, Japan, 1990;

1355  pp 203−233.

R.; Zong, Z. M. Green and effective catalytic hydroconversion of an  1422

extractable portion from an oil sludge to clean jet and diesel fuels over a 1423

- https://doi.org/10.1021/acs.energyfuels.3c01713

1424  mesoporous  Y  zeolite-supported  nickel  catalyst.  Fuel  2021, 287,

1425  119396.

(107) Gong, W. B.; Chen, C.; Zhang, H. M.; Zhang, Y.; Zhang, Y. X.; 1492

Wang, G. Z.; Zhao, H. J. Selective liquid phase hydrogenation of furfural 1493

1426

- Gao, J.; Wei, X. Y.; Kang, Y. H.; Zhang, X. Q.; Wang, A. M.; Li, X.

to furfuryl alcohol by Ru/Zr-MOFs. J. Mol. Catal. A-Chem. 2017, 429, 1494

1427 L.; Gao, Y.; Liu, G. H.; Chen, T.; Li, Y. J.; Ma, X. R.; Bai, J. J.; Bai, N.;

51−59.

1495

1428 Ma, Y. J.; Zong, Z.  M.  Mesoporous  zeolite  Beta  supported  Ni 1429 nanoparticles for the catalytic hydroconversion of extraction portion 1430 from Jinjitan subbituminous coal to cycloalkanes. Fuel 2023, 339,

(108) Wang, Y.; Miao, Y. N.; Li, S.; Gao, L. J.; Xiao, G. M. Metal- 1496 organic frameworks derived bimetallic Cu-Co catalyst for efficient and 1497 selective hydrogenation of biomass-derived furfural to furfuryl alcohol. 1498

1431  127435.

Mol. Catal. 2017, 436, 128−137.

1499

1432

- Li, L.; Wei, X. Y.; Shao, C. W.; Li, Z.; Li, J. H.; Fan, Z. C.; Lu, K.

(109) Ma, Y. F.; Xu, G. Y.; Wang, H.; Wang, Y. X.; Zhang, Y.; Fu, Y. 1500

1433  L.; Liu, F. J.; Kong, Q. Q.; Zhao, J.; Liu, Z. Q.; Zong, Z. M. Catalytic

1434 hydroconversion of an organic waster oil to cyclanes over a supported

Cobalt nanocluster supported on zrrenox for the selective hydro- 1501

genation of biomass derived aromatic aldehydes and ketones in water. 1502

1435 nickel catalyst. Fuel 2023, 331, 125697.

ACS Catal. 2018, 8 (2), 1268−1277.

1503

1436

(92) Li, L.; Wei, X. Y.; Liu, G. H.; Li, Z.; Li, J. H.; Liu, F. J.; Kong, Q.

- Zhang, J.; Dong, K. J.; Luo, W. N.; Guan, H. F. Selective transfer 1504

1437  Q.;  Fan,  Z.  C.;  Zong,  Z.  M.;  Bai,  H.  C.  Selective       catalytic

1438  hydroconversion of organic waster oil to cyclanes over a coal fly ash-

hydrogenation  of  furfural  into  furfuryl  alcohol  on  Zr-containing 1505

catalysts using lower alcohols as hydrogen donors. ACS Omega 2018, 1506

1439 derived zeolite-supported nickel catalyst: Waster to energy. Fuel 2022,

3 (6), 6206−6216.

1507

1440  316, 123185.

- Jia, P.; Lan, X. C.; Li, X. D.; Wang, T. F. Highly active and 1508

1441

(93) Chen, B.; Guo, H.; Wan, Z.; Xu, X.; Zhang, H.; Zhao, D.; Chen,

selective NiFe/SiO2 bimetallic catalyst with optimized solvent effect for 1509

1442 X.; Zhang, N. Efficient catalytic hydrogenation of butyl levulinate to γ-

the liquid-phase hydrogenation of furfural to furfuryl alcohol. ACS 1510

1443  valerolactone over a stable and magnetic CuNiCoB amorphous alloy

Sustainable Chem. Eng. 2018, 6 (10), 13287−13295.

1511

1444 catalyst. Energy Fuels 2018, 32 (4), 5527−5535.

(112) Nandi, S.; Saha, A.; Patel, P.; Khan, N. H.; Kureshy, R. I.; Panda, 1512

1445

- Scotti, N.; Dangate, M.; Gervasini, A.; Evangelisti, C.; Ravasio,

A. B. Hydrogenation of furfural with nickel nanoparticles stabilized on 1513

1446 N.; Zaccheria, F. Unraveling the role of low coordination sites in a Cu

1447  metal nanoparticle: A step toward the selective synthesis of    second

nitrogen-rich  carbon  core−shell  and  its  transformations  for  the   1514

synthesis of γ-valerolactone in aqueous conditions. ACS Appl. Mater. 1515

1448 generation biofuels. ACS Catal. 2014, 4 (8), 2818−2826.

Interfaces 2018, 10 (29), 24480−24490.

1516

1449

- Mariscal, R.; Maireles-Torres, P.; Ojeda, M.; Sádaba, I.; López-

(113) Xie, L. F.; Chen, T.; Chan, H. C.; Shu, Y. J.; Gao, Q. S. 1517

1450 Granados, M. Furfural: a renewable and versatile platform molecule for

1451 the synthesis of chemicals and fuels. Energy Environ. Sci. 2016, 9 (4),

Hydrogen  doping  into  MoO3   supports  toward  modulated  metal- 1518

support interactions and efficient furfural hydrogenation on iridium   1519

1452  1144−1189.

nanocatalysts. Chem. Asian J. 2018, 13, 641−647.

1520

1453

(96) Lange, J. P.; van der Heide, E.; van Buijtenen, J.; Price, R.

(114) Jiang, P. B.; Li, X. L.; Gao, W. B.; Wang, X.; Tang, Y.; Lan, K.; 1521

1454 Furfural�A promising platform for lignocellulosic biofuels.   Chem-

1455  SusChem 2012, 5 (1), 150−166.

Wang,  B.; Li,  R. Highly  selective hydrogenation of  α,β-unsaturated 1522

carbonyl compounds over supported Co nanoparticles. Catal. Commun. 1523

1456

- Bohre, A.; Dutta, S.; Saha, B.; Abu-Omar, M. M. Upgrading

2018, 111, 6−9.

1524

1457 furfurals to drop-in biofuels: an overview. ACS Sustain. Chem. Eng.

1458  2015, 3 (7), 1263−1277.

(115) Chen, H.; Ruan, H. H.; Lu, X. L.; Fu, J.; Langrish, T.; Lu, X. Y. 1525

Efficient catalytic transfer hydrogenation of furfural to furfuryl alcohol 1526

1459

- Addepally, U.; Thulluri, C. Recent progress in production of fuel

in near-critical isopropanol over Cu/MgO-Al2O3 catalyst. Mol. Catal. 1527

1460 range liquid hydrocarbons from biomass-derived furanics via strategic

2018, 445, 94−101.

1528

1461 catalytic routes. Fuel 2015, 159, 935−942.

(116) Wu, J.; Zhang, X.; Chen, Q.; Chen, L.; Liu, Q.; Wang, C.; Ma, L. 1529

1462

- Guzmán, I.; Heras, A.; Güemez, M. B.; Iriondo, A.; Cambra, J. F.;

One-pot  hydrogenation  of  furfural  into  tetrahydrofurfuryl  alcohol 1530

1463 Requies, J. Levulinic acid production using solid-acid catalysis. Ind. Eng.

under ambient conditions over PtNi alloy catalyst. Energy Fuels 2020, 1531

1464 Chem. Res. 2016, 55 (18), 5139−5144.

34 (2), 2178−2184.

1532

1465

- Audemar, M.; Ciotonea, C.; De Oliveira Vigier, K.; Royer, S.;

(117) Li, Z. X.; Wei, X. Y.; Yang, Z.; Zhang, M.; Niu, S.; Meng, X. L.; 1533

1466  Ungureanu,  A.;  Dragoi,  B.;  Dumitriu,  E.;  Jerome,  F.     Selective

1467 Hydrogenation of furfural to furfuryl alcohol in the presence of a

Li, J.; Zong, Z.-M. Highly selective hydrogenation of furfural to furan-2- 1534

ylmethanol over a Cu/C derived from copper-organic frameworks.    1535

1468 recyclable cobalt/SBA-15 catalyst. ChemSusChem 2015, 8 (11), 1885−

Catal. Commun. 2019, 129, 105679.

1536

1469  1891.

(118)

Maderuelo-Solera,  R.;  López-Asensio,  R.;  Cecilia,  J.  A.;    1537

1470

- Yuan, Q. Q.; Zhang, D. M.; Haandel, L. V.; Ye, F. Y.; Xue, T.;

Jiménez-Gómez,  C.  P.;  García-  Sancho,  C.;  Moreno-Tost,  R.;    1538

1471  Hensen, E. J. M.; Guan, Y. J. Selective liquid phase hydrogenation of

1472 furfural to furfuryl alcohol by Ru/Zr-MOFs. J. Mol. Catal. A-Chem.

Maireles-Torres, P. Catalytic transfer hydrogenation of furfural to 1539

furfuryl alcohol over calcined MgFe hydrotalcites. Appl. Clay Sci. 2019, 1540

1473  2015, 406, 58−64.

183, 105351.

1541

1474

- Fulajtárova, K.; Soták, T.; Hronec, M.; Vávra, I.; Dobrocka, E.;

(119) Li, Z. X.; Wei, X. Y.; Yang, Z.; Zhang, M.; Meng, X. L.; Niu, S.; 1542

1475  Omastová, M. Aqueous phase hydrogenation of furfural to   furfuryl

1476 alcohol over Pd-Cu catalysts. Appl. Catal. A-Gen. 2015, 502, 78−85.

Zhang, D.; Zong, Z. M. Highly selective hydrogenation of furfural to 1543

furan-2-ylmethanol over ZIF-67-templated magnetic Cu-Co/C. Catal. 1544

1477

- Wang, F.; Zhang, Z. H. Catalytic transfer hydrogenation of

Lett. 2020, 150 (1), 178−184.

1545

1478 furfural into furfuryl alcohol over magnetic γ-Fe2O3@HAP   catalyst.

1479 ACS Sustainable Chem. Eng. 2017, 5 (1), 942−947.

(120) Xu, L.; Nie, R.; Lyu, X.; Wang, J.; Lu, X. Selective hydrogenation 1546

of furfural to furfuryl alcohol without external hydrogen over N-doped 1547

1480

- Gong, W. B.; Chen, C.; Zhang, Y.; Zhou, H. J.; Wang, H. M.;

carbon confifined Co catalysts. Fuel Process. Technol. 2020, 197, 1548

1481 Zhang, H. M.; Zhang, Y. X.; Wang, G. Z.; Zhao, H. J. Efficient synthesis

106205.

1549

1482 of furfuryl alcohol from H2-hydrogenation/transfer hydrogenation of 1483 furfural using sulfonate group modified Cu catalyst. ACS Sustainable 1484 Chem. Eng. 2017, 5 (3), 2172−2180.

(121) Li, Z. X.; Wei, X. Y.; Liu, G. H.; Meng, X. L.; Yang, Z.; Niu, S.; 1550 Zhang, D.; Gao, H. S.; Ma, Z. H.; Zong, Z. M. Highly selective 1551 hydrogenation  of  furfural  and  levulinic  acid  over  Ni0.09Zn/NC600 1552

1485

- Dohade, M. G.; Dhepe, P. L. Efficient hydrogenation of

derived from ZIFW-8. Mol. Catal. 2020, 480, 110651.

1553

1486 concentrated aqueous furfural solutions in to furfuryl alcohol under 1487 ambient conditions in presence of PtCo bimetallic catalyst. Green Chem. 1488  2017, 19, 1144−1154.

(122) Li, Z. X.; Wei, X. Y.; Yang, Z.; Li, J.; Yan, W. W.; Bie, L. L.; 1554 Zhang, Y. Y.; Zong, Z. M.; et al. Selective hydrogenation of bio-based 1555 furfural over Co-based catalysts derived from zeolitic imidazolate frame 1556

1489

- Wu, J.; Gao, G.; Li, J. L.; Sun, P.; Long, X. D.; Li, F. W. Efficient

materials. Mol. Catal. 2020, 492, 111007.

1557

1490  and  versatile  CuNi  alloy  nanocatalysts  for  the  highly     selective

(123)

Borah,  P.;  Yamashita,  Y.;  Kobayashi,  S.  Solid  superbase- 1558

1491 hydrogenation of furfural. Appl. Catal., B 2017, 203, 227−236.

catalyzed stereoselective 1,4-addition reactions of simple amides in 1559

- https://doi.org/10.1021/acs.energyfuels.3c01713

1560 batch and continuous-flow systems. Adv. Synth. Catal. 2019,    361,

1561  3807−3812.

(142) Wang, D.; Wang, Y.; Li, X.; Chen, L.; Li, G.; Li, X. Lignin 1629

Valorization: A novel in situ catalytic hydrogenolysis method in alkaline 1630

1562

- Li, M.; Wang, S.; Li, F.; Zhou, L.; Lei, L. Iodine-mediated

aqueous solution. Energy Fuels 2018, 32 (7), 7643−7651.

1631

1563  photo-controlled atom transfer radical polymerization (photo-ATRP)

1564 and block polymerization combined with ring-opening polymerization

(143) Reynoso, A. J.; Ayastuy, J. L.; Iriarte-Velasco, U.; Gutiérrez-    1632

Ortiz, M. A. Cobalt aluminate spinel-derived catalysts for glycerol 1633

1565 (ROP) via a superbase. Polym. Chem. 2020, 11, 6591−6598.

aqueous phase reforming. Appl. Catal. B Environ. 2018, 239, 86−101.

1634

1566

- Shigeno, M.; Hayashi, K.; Korenaga, T.; Nozawa-Kumada, K.;

(144) Morales-Marín, A.; Ayastuy, J. L.; Iriarte-Velasco, U.; Gutiérrez- 1635

1567 Kondo, Y. Organic superbase t-bu-P4-catalyzed demethylations     of

1568 methoxyarenes. Org. Chem. Front. 2022, 9, 3656−3663.

Ortiz, M. A. Nickel aluminate spinel-derived catalysts for the aqueous 1636

phase reforming of glycerol: Effect of reduction temperature. Appl.   1637

1569

- Zhang, F. C.; Zhang, Q. X.; Liu, P.; Zhang, K.; Ji, K. M.; Zhang,

Catal. B Environ. 2019, 244, 931−945.

1638

1570 J. L.; Zhao, L.; Song, Q. W. Selective synthesis of dimethyl carbonate via

1571 the coupling reaction of CO2 and alcohols by the synergistic catalysis of

1572 silver sulfadiazine and superbase. J. Fuel Chem. Technol. 2023, 51, 304−

1573  312.

(145) Zhang, X. Q.; Kang, Y. H.; Gao, J.; Xiong, L.; Gao, Y.; Chen, T.; 1639 Liu, G. H.; Wang, A. M.; Wei, X. Y.; Zong, Z. M.; Bai, H. C. Effective 1640 hydroconversion of heteroatom-containing organic species from the 1641 extraction of low-temperature coal tar to cycloalkanes over a Y/Beta  1642

1574

- Wang, Z.; Wang, Z.; Huang, X.; Yang, D.; Wu, C.; Chen, J. Deep

composite zeolite supported nickel nanoparticles. Fuel 2022, 321, 1643

1575 eutectic  solvents  composed  of  bio-phenol-derived  superbase ionic

124062.

1644

1576 liquids and ethylene glycol for CO2 capture. Chem. Commun. 2022, 58,

1577  2160−2163.

(146) Liu, G. H.; Bai, J. J.; Lu, K. L.; Kan, H.; Zhang, X. Q.; Kang, Y. 1645

H.; Lu, C. Y.; Li, Z. K.; Bai, H. C.; Wei, X. Y. Integrated catalytic 1646

1578

- Ishaq, M.; Gilani, M. A.; Arshad, I.; Bilad, M. R.; Ahmad, F.;

hydroconversion of three crop stalks to valuable oxygenated organic  1647

1579 Khan, A. L. Synergy of high permeability and selectivity of superbase/

chemicals. Fuel 2022, 322, 124149.

1648

1580  choline  chloride/urea  solution  impregnated  membranes  for  CO2

1581 capture. Carbon Capture Sci. Technol. 2021, 1, 100019.

(147) Li, L. Catalytic hydroconversion of Runbei lignite and Shaerhu 1649

subbituminous coal. Doctoral dissertation of China University of Mining 1650

1582

- Li, W. T.; Wei, X. Y.; Li, X. K.; Liu, X. X.; Li, Z. K.; Zong, Z. M.

& Technology 2023, Xuzhou, Jiangsu, China.

1651

1583  Catalytic hydroconversion of lignite-related model compounds  over

1584 difunctional Ni-Mg2Si/-Al2O3. Fuel 2017, 200, 208−217.

(148) Wei, X. Y.; Zong, Z. M.; Zhao, W.; Ni, Z. H.; Cao, J. P.; Fan, X.; 1652

Zhao, Y. P.; Liu, Z. W.; Peng, Y. L.; Liang, J.; Zhao, X. Y.; Tao, X. Y.; 1653

1585

- Liu, Z. Q.; Wei, X. Y.; Liu, F. J.; Liu, G. H.; Zong, Z. M. Catalytic

Kang, Y. H.; Mo, W. L.; Cong, X. S.; Wang, Y. G.; Liu, Z. Q.; Liu, G. H.; 1654

1586  hydroconversion of Yiwu lignite over solid superacid and superbase.

1587 Fuel 2019, 238, 473−482.

Guo, X. H.; Ma, Z. H.; Gao, H. S.; Li, J. H.; Chen, Y. F.; Yan, W. W.; Yin, 1655

F.; Jiang, Z. J.; Yu, X. K. Basic research and technology development for 1656

1588

- Liu, X. X.; Zong, Z. M.; Li, W. T.; Li, X.; Li, Z. K.; Wang, S. K.;

the separation of condensed aromatics from high-temperature coal tar. 1657

1589 Wei, X. Y. A recyclable and highly active magnetic solid superbase for

Acta Petrolei Sinica (Petroleum Processing Section) 2022, 38 (3), 500− 1658

1590 hydrocracking C-O bridged bonds in sawdust. Fuel Process. Technol.

511.

1659

| 1591 2017, 159, 396−403. 1592 (132) Zhang, M.; Wei, X. Y.; Yang, Z.; Teng, D. G.; Xue, Y.; Meng, D. 1593 W.; Zong, Z. M. Catalytic hydroconversion of the extraction residue 1594 from Naomaohu lignite over an active and separable magnetic solid 1595 superbase. Fuel 2018, 226, 410−416. 1596 (133) Xu, M. L.; Wei, X. Y.; Liu, G. H.; Li, F. H.; Zhao, Y. P.; Liu, F. J.; 1597 Li, S.; Zong, Z. M.; Fan, X.; Cao, J. P.; Zhao, W.; Ma, F. Y.; Liu, J. M. 1598 Directional catalytic hydroconversion of oxybis(methylene)dibenzene 1599 and extract from Piliqing subbituminous coal over a magnetic 1600 difunctional solid superbase. ChemistrySelect 2020, 5, 1130−1134. 1601 (134) Xu, M. L.; Wei, X. Y.; Wu, Q. C.; Zhao, Y. P.; Li, F. H.; Liu, G. 1602 H.; Liu, F. J.; Zong, Z. M.; Zhang, M.; Li, S.; Fan, X.; Zhao, W.; Ma, F. 1603 Y.; Mo, W. L.; Liu, J. M. Enhanced hydrogenation of aromatic rings and 1604 hydrocracking of > Car-O- bridged bonds in the extraction residue from |  | - Wei, X. Y. Directional conversion of carbon resources to 1660 advanced materials. Symposium on integrated production technology for 1661 the deep processing of new chemical materials and their downstream 1662 products; Ordos, China, 2023. 1663 - Shi, D. L.; Wei, X. Y.; Fan, X.; Zong, Z. M.; Chen, B.; Zhao, Y. 1664 P.; Wang, Y. G.; Cao, J. P. Characterizations of the extracts from Geting 1665 bituminous coal by spectrometries. Energy Fuels 2013, 27 (7), 3709− 1666 3717. 1667 - Gao, Y.; Wei, X. Y.; Li, Y. J.; Bai, J. J.; Kang, Y. H.; Liu, G. H.; 1668 Ma, X. R.; Li, X.; Lu, C. Y.; Bai, H. C.; Zong, Z. M. Investigation on the 1669 composition of soluble portions from the extraction residue of 1670 Hanglaiwan subbituminous coal by thermal dissolution and alkanol- 1671 yses. Fuel 2021, 306, 121747. 1672 - Liu, Z. W.; Zong, Z. M.; Li, J. N.; Chen, C. F.; Jiang, H.; Peng, Y. 1673 |
| --- | --- | --- |
| 1605 Piliqing subbituminous coal over a magnetic difunctional solid |  | L.; Xue, J. Q.; Yang, X. L.; Zheng, Y. X.; Zhou, X.; Xie, R. L.; Wei, X. Y. 1674 |
| 1606 superbase. J. Anal. Appl. Pyrolysis 2020, 146, 104695. |  | Isolation and identification of two bis(2-ethylheptyl) benzenedicarbox- 1675 |
| 1607 (135) Liu, F. J.; Guo, J. P.; Liu, G. H.; Bie, L. L.; Zhao, Y. P.; Huang, Z. |  | ylates from Lingwu coal. Energy Fuels 2009, 23 (1), 588−590. 1676 |
| 1608 X.; Wei, X. Y. Effect of temperature on catalytic hydrocracking of |  | (153) Zong, Y.; Zong, Z. M.; Ding, M. J.; Zhou, L.; Huang, Y. G.; 1677 |
| 1609 Xiaolongtan lignite over a mesoporous silica-coated Fe3O4 supported 1610 magnetic solid base for producing aromatics. J. Energy Inst. 2021, 94, |  | Zheng, Y. X.; Jin, X.; Ma, Y. M.; Wei, X. Y. Separation and analysis of 1678 organic compounds in an Erdos coal. Fuel 2009, 88 (3), 469−474. 1679 |
| 1611 352−359. |  | (154) Liu, Z. W.; Wei, X. Y.; Zong, Z. M.; Li, J. N.; Xue, J. Q.; Chen, X. 1680 |
| 1612 (136) Mathews, J. P.; Chaffee, A. L. The molecular representations of |  | F.; Chen, F. J. Isolation and identification of methyl alkanoates from 1681 |
| 1613 coal - A review. Fuel 2012, 96, 1−14. |  | Lingwu coal. Energy Fuels 2010, 24 (4), 2784−2786. 1682 |
| 1614 (137) Liu, F. J.; Wei, X. Y.; Fan, M. H.; Zong, Z. M. Separation and |  | (155) Cong, X. S.; Zong, Z. M.; Zhou, Y.; Li, M.; Wang, W. L.; Li, F. 1683 |
| 1615 structural characterization of the value-added chemicals from mild |  | G.; Zhou, J.; Fan, X.; Zhao, Y. P.; Wei, X. Y. Isolation and identification 1684 |
| 1616 degradation of lignites: A review. Appl. Energy 2016, 170, 415−436. |  | of 3-ethyl-8-methyl-2,3-dihydro-1H-cyclopenta[a]- chrysene from 1685 |
| 1617 (138) Liu, G. H.; Li, Y. J.; Bai, J. J.; Gao, Y.; Kang, Y. H.; Wang, A. M.; |  | Shengli lignite. Energy Fuels 2014, 28 (10), 6694−6697. 1686 |
| 1618 Lu, C. Y.; Bai, H. C.; Zong, Z. M.; Wei, X. Y. Advances in mild |  | (156) Cong, X. S.; Zong, Z. M.; Wei, Z. H.; Li, Y.; Fan, X.; Zhou, Y.; Li, 1687 |
| 1619 degradation and directional upgrading of lignites: From feature |  | M.; Zhao, Y. P.; Wei, X. Y. Enrichment and identification of arylhopanes 1688 |
| 1620 identification to value-added utilization. J. Anal. Appl. Pyrolysis 2022, |  | from Shengli lignite. Energy Fuels 2014, 28 (11), 6745−6748. 1689 |
| 1621 163, 105477. |  | (157) Cong, X. S.; Zong, Z. M.; Li, M.; Zhou, Y.; Gao, S. Q.; Wei, X. Y. 1690 |
| 1622 (139) Benson, S. W. Bond energies. J. Chem. Educ. 1965, 42, 502−508. |  | Isolation and identification of two novel condensed aromatic lactones 1691 |
| 1623 (140) Kerr, J. A. Bond dissociation energies by kinetic methods. Chem. |  | from Zhundong subbituminous coal. Energy Fuels 2014, 28 (12), 1692 |
| 1624 Rev. 1966, 66, 465−500. |  | 7394−7397. 1693 |
| 1625 (141) Liu, G. H.; Qi, Y. C.; Wang, H.; Wang, A. M.; Kang, Y. H.; Gao, |  | (158) Cong, X. S.; Zong, Z. M.; Zhou, Y.; Li, M.; Zhao, Y. P.; Fan, X.; 1694 |
| 1626 Y.; Bai, N.; Li, Z. K.; Wei, X. Y. Synergistic transfer of active hydrogen in |  | Wei, X. Y. Enrichment and analysis of long-chain normal alkanals from 1695 |
| 1627 the catalytic hydroconversion of lignite-derived aryl ethers to cyclanes: |  | Zhundong subbituminous coal. J. Fuel Chem. Technol. 2014, 42 (3), 1696 |
| 1628 A combined experimental and DFT study. Fuel 2023, 351, 129034. |  | 257−261. 1697 |
|  | S | https://doi.org/10.1021/acs.energyfuels.3c01713 |

1698

- Cong, X. S.; Zong, Z. M.; Li, M.; Gao, L.; Wei, Z. H.; Li, Y.; Fan,

1699 X.; Zhou, Y.; Wei, X. Y. Enrichment and identification of cyclized

1700 hopanoids from Shengli lignite. Fuel Process. Technol. 2015, 134, 399−

1701  403.

1702

- Liu, G. H.; Zong, Z. M.; Liu, F. J.; Meng, X. L.; Zhang, Y. Y.;

1703 Wang, S. K.; Li, S.; Zhu, C.; Wei, X. Y.; Ma, F. Y.; Liu, J. M. Deep

1704 hydroconversion of ethanol-soluble portion from the ethanolsis of 1705 Dahuangshan lignite to clean liquid fuel over a mordenite supported 1706 nickel catalyst. J. Anal. Appl. Pyrolysis 2019, 139, 13−21.

1707

- Guan, Y. S.; Zhao, W.; Zhao, C.; Wang, D. K.; Ao, L.; Liu, K. S.;

1708 Liu, H. M.; Chen, S. L.; Fan, X.; Wei, X. Y. A novel magnetic solid acid 1709 for specially cleaving  the  C-O  bridged  bond  in  dibenzyl  ether. 1710 ChemistrySelect 2018, 3 (41), 11610−11615.

1711

- Zhao, M. X.; Wei, X. Y.; Qu, M.; Li, Z. K.; Liu, J.; Li, Y.; Kong, J.;

1712 Zhao, W.; Zong, Z. M. Hydrocracking of benzyloxybenzene as a lignite- 1713 related model compound over a novel solid acid. Fuel Process. Technol. 1714  2016, 146, 110−115.

T	https://doi.org/10.1021/acs.energyfuels.3c01713